# VOLUME 3

# TECHNICAL SPECIFICATIONS

PLACING TAMPON LAYER MADE OF DEBRIS STONE AGGREGATE

0-63mm and 0-31,5mm

Description

Position contains procurement, transportation, roughly and fine spreading, eventually

Watering, compressing layer made of debris stone material, according to dimensions given in project design.

Construction

Construction is being done in one or two layers depending from mechanization. Material has to be spreader in longitudinal direction and slope equal to vertical alignment. In cross section it has to have lope of existing vertical alignment, apropos necessary for draining atmosphere water.

Layer has to compress in full width (apropos width of driving lane) with right compressing tool. Compressing should be doing form lower to higher edge.

Material for bearing course mustn’t be placed over frozen surface, either be placed over layers of snow or ice.

Quality control of material used for bearing layer made of debris stone

For construction of Bottom Bearing Course have to be placed debris stone aggregate. Quality control over previously examinations supposed to be done according to next regulations:

SRPS B.B8. 001 – Natural aggregate and stone, taking of samples,

SRPS B.B8. 012 – Natural stone, testing of pressure resistance,

SRPS B.B8. 010 – Determination of water absorbed by natural stone,

SRPS B.B8. 020 – Testing of durability of stone on frost,

SRPS B.B8.045– Testing of resistance of stone and stone aggregate to wearing in accordance with Los Angeles method

SRPS B.B8. 037 – Determination of brittle grains in large aggregate (gravel)

SRPS B.B8. 047 – Definition of forms and appearance of the stone aggregate grain surface,

SRPS B.B8. 048 –Testing of the form of the aggregate grains

SRPS B.B8. 018 – Determination of grading composition and determination, in accordance with item 5,of the particles of 0,02mm by aerometry (or as per SRPS B.B8.036)

SRPS B.B8. 036 – Determination of quantity of particles in aggregate which pass though the

sieve of 0,02mm opening (the method from this SRPS-a)

SRPS B.B8. 038 – Content of clay and mud ingredients,

SRPS B.B8. 031 – Absorption of aggregate water,

SRPS B.B8. 030 – Volume weight with pore and cavities (in compressed and loose conditions) aggregate,

SRPS B.B80. 032 – Stone volume weight (with pores and cavities and without them) and porosity and density of stone,

SRPS B.B8 012 – Determination of soil moisture,

SRPS B.B8 016 – Determination of volumetric weight and water absorption with aggregate (gravel),

SRPS B.B8 038 –  Determination of optimum water content in the soil,

SRPS B.B8 042 –  Determination of Californian index of load capacity

Examination is being done for every material change.

Criterion for grading material for bearing course

Debris stone aggregate made of grains of crushed stone, chippings, sand and fill out material have to reach certain demands in range:

-Physical-mechanical and mineralogical-petrographic characteristic of rock itself and aggregate

-grading composition of all material

-content of organic materials and light particles

Crushed material for mechanical stabilized bottom bearing courses have to be made of grains which are appropriate to next condition:

Physical-mechanical characteristics of the rock

Mid-solidity pressure resistance (Mpa)

- in dry conditions min. 120

-water absorption (% mass) 1,0

-consistency on freezing if mid-solidity pressure resistance after freezing to 20% according to mid pressing solidity in dry condition).

Mineralogical-petrographic composition

Rock can be eruptive, sedimentary and metamorphic source.

Physical-mechanical performance of crushed stone aggregate

- Grain shape, part of grain unfavorable shape (3:1) - max. 40%

- Water absorption (SRPS b.b8. 031 - max. 1.6%)

- Brittle grain – max. 7%

- Resilience on wearing by Los Angeles method – max 40%

- Content mud-clay muddy and organic particle – max. 5%

Note: On non-separated stone materials with regular limit value for part of appropriate shape, brittle non-quality grains, water absorption, loss on NA2SO4 grains are calculation in percent of mass on laboratory separated fractions, apropos part of grains bigger than 4mm.

On separated stone materials of regulated limit value are expressing in percent of mass on tested – rated fraction.

Beside mentioned criteria, material has to acquire and next demands:

- Content of grains smaller than 0,02mm mustn’t be bigger than 3%.

Control of treated an compressed bearing course

Control of treated and compressed bottom bearing course is being by determination of grade of compression or module of compressibility on each 300m2. If it is doing parallel determination grade of compression and module compressibility, testing is being done on each 50m.

Minimal demanded values from module of compressibility Ms measured with circular plate ø30cm, must be 80Mpa for 0-31,5mm and 60Mpa for 0-63mm.

Testing is being done by next regulative:

SRPS U.B1. 010 – taking samples

SRPS U.B1. 012 – determine humidity

SRPS U.B1. 016 – determine volume weight.

BUILDING BITUMIOUS BEARING COURSE BNS 22

Description

Position including procurement, preparation, placing and compressing of mixture made of granulated mineral material and bitumen, in one layer, necessary thickness according to project.

Base materials

For building top bearing course made of bituminous material should apply next base materials:

- crushed carbonate stone material  0/4; 4/8; 8/16; 16/22; 22/32mm;

- stone flour carbonate composition.

- connective BIT 60

Base materials quality

Rocky chippings

Rocky chippings should be made of carbonate stone mass which has next performance:

- solidity on pressure in dry and water saturated condition 120 MPa

- on freeze stability – fall mid- compressibility after 25 cycle max. 20%

Rocky chippings should satisfy next conditions:

- wearing by Los Angeles – max 28%

- grains undesired shape – max 20%

- content dusty particles under 0,09mm –max 5%

- aggregate surface coverage with bitumen – min 100/80

- water absorbing on fraction  4/8mm  1,2%

Rocky flour

Rocky flour has to be by adequately criteria given in SPRS B.3.045 for 1st quality class

Bitumen

Bitumen BIT 60 in everything has to appropriate by criteria given in SRPS U.M3.010.

Mixture

In asphalt mixture usage of bitumen should be approximate 3.5%. Exact content of bitumen will be determined in pre-content of asphalt mixture.

Characteristics of tested samples by Marshall procedure have to be next:

- content of cavities (vl%) – 3-9%

- stability (Kh) – min 6,0

- cavity fil out with bitumen mineral mixture – 50-70% .

TECHNOLOGY OF EXECUTION

Surface preparation

Asphalt layer can be placed on surface which is dry and which mustn’t be frozen in any case. Before work start has to well cleaned with steel brush and blown by compressor. After Surface cleaning is done Supervisor will record vertical alignment and surface flatness. On parts where layer surface is out of regulated height for more than +15mm is necessary for contractor do fixing of surface according to demands wanted in project solution, regarding:

- on places where area of surface is under regulated vertical alignment supposed to do fix

by increasing layer of asphalt mixture with asphalt concrete –wearing course;

- on places where area of surface above provided vertical alignment it’s necessary to take

off extra asphalt mass in surface rototillings.

Preparation and transport of asphalt mixture

Asphalt mixture have to posses griddle with hatch 45mm,regarding 32mm by which will be removing non allowed large grains in mineral mixture. Temperature of bitumen need to be between 150 and 165 ° C. Aggregate temperature mustn’t be higher than bitumen temperature for more than 15°C. Temperature of asphalt mixture in mixer need to be in limits between 150- 170°C. (exceptionally 175°C).

Placing asphalt mixture

Temperature of asphalt mixture on a place of placing musn’t be lower than 140°C and higher than 160°C.

Period of work execution

Wearing layer with specification from this technical conditions can be placed only in period from 15th of April to 15th of October, regarding to period when air temperature higher than 5°C,without wind or min 10°C with wind.

Placing of asphalt mixture mustn’t be doing when there is mist or rain.

Surface temperature mustn’t be lower than +5°C.

QUALITY CONTROL

Previously done examination of asphalt mixture

Before work start contractor is obligated to make in official laboratory project previous asphalt mixture in everything agreeable with demands these technical conditions.

None work mustn’t be started until contractor suggests previous mixture on agreement to Supervisor. Certificate of base materials and previous mixture mustn’t be older than 6 months. In case that changes show up in base materials or if choice of material is changed, Contractor’s duty to suggest Supervisor in written form with suggestion for changing of asphalt mixture regarding to suggest new previous mixture on agreement, before start using those materials.

Proven work composition of asphalt mixture

Quality of previous asphalt mixture proving with probation with the fact that asphalt mixture taking on the very plant, and quality of placing on request part. If quality of base materials on construction site doesn’t fit these technical conditions, Contractor’s duty is to supply new quality base materials. If dozing of base materials, according previous mixture, can’t satisfy all regulated demands for physical-mechanical feature of asphalt mixture and for placed layer, it’ s necessary to do correction of dosage of base materials and repeat probation. Only when with probation achieve all set demands, Supervisor will adopt work mixture and give agreement for non-stop work.

Proven work composition of asphalt mixture is being done operation by authorized laboratory.

Quality control

For security of regulated quality in process of building investor or form it engaged laboratory will execute by regular examine control such as:

Bitumen examination

Contractor can procure bitumen only under condition that for every delivery provide certificate of manufacturer which will be deliver at the moment to Supervisor on review, regarding to the laboratory.

Beside review of manufacturer’s certificate, operational laboratory will run regular tests in short form (,PK’’ , penetration, and breaking point) and so:

- on work start and

- on each 500t of supplied bitumen

Filer testing

Laboratory will test grading filer composition:

- on work start

- on each 100t of delivered filer.

Testing of physical- mechanical characteristic of asphalt mixture of placed layer,

These tests will do operational laboratory:

- on work start, and

- on each 2000m2

Sample of asphalt mass is taking from just spreaded asphalt mixture behind finisher. Compressibility control and cavities in road is being done by taking kern from done layer on the same place where sample of hot asphalt mixture was taken.

BUILDING OF WEARING LAYER OF ASPHALT CONCRETE AB 11

Description

Position contains procurement, mixing, placing and compressing of asphalt concrete in to designed thickness of layer.

Base for making of technical conditions for position is SRPS.U.E4.014

Base materials:

- crushed noble rock chippings 2/4mm, 4/8mm, 8/11mm:

- crushed sand 0/2mm (carbonate)

- crushed flour carbonate composition

- bitumen BIT 60 (PK=49-55; Pen=50-70).

Base materials quality

Rocky chippings

Rocky chippings should be made of stone mass which has next:

Compressibility stability – min 140 MPa

Wearing by grinding – max. 18cm3/50 cm2

Constancy to –freezing of good.

Fall of mid compressibility stability after 25 cycles of freezing and curving max 20%

Rocky chippings have to satisfy next conditions:

- Grading composition of fraction according to SRPSU. E4 014/90

- Wearing by Los Angeles ….......................................max 18%

- Grains content of unwanted shape ………………………… max 20%

- Content of brittle grains………………………………………… max   3%

- Content of clay nubs in single fractions according to SRPS B.BB.038 – max 0,25%

- Surface aggregate coverage with bitumen – min. 100/90 (SRPSU.M8.096).

Sand

For san can be used noble crushed stone, crushed from stone mass made of carbonate composition.

Sand has to satisfy next performance:

- Equivalent of sand is min 60%

- In sand mustn’t be clay nubs

- Sand mustn’t contain organic filth

- In sand mustn’t create nubs of  glued particles

Stone flour

For stone flour need to apply carbonate stone flour 1st class quality according to SRPS.B.3045 It isn’t advisable usage of stone flour made of minced dolomite stone because of bad connectivity for concrete.

Before work start contractor need to get certificate from authorized laboratory about stone flour quality which will guarantee quality according to standard SRPSSB.B3045(1.Quality)

Bitumen

For connection should apply BIT 60 with: softening point (ring and pellet PK95-55°C), returning to previous 50-70, and penetration index bigger than – 1.0, content of paraffin max 2% and ductility min 100cm. Rest of compositions according to SRPSU.M3.010.

Optimal quantity of bitumen in asphalt mixture shouldn’t be less than 5,0% to prevent quick fatigue of asphalt concrete.

At stone chippings coming from stone masses which use small quantity of bitumen for coverage, so that optimal quantity be under 5% it’s necessary to apply bottom limit value of line of sieve in area of filter and sand, and bottom value of sieve in area of stone chippings.

Physical-mechanical performance of asphalt mixture

Asphalt mixture compressed in Marshall molds on 147-153°C and mineral mixture made of extraction asphalt mass need to satisfy next conditions:

Performance placed asphalt layer

Placed layer made of asphalt concrete has to have next performance:

- Unfiled cavities (5)    			3-7

- Distance (compressed) layer (%)         min 97

- Layer flatness under levelers 4m          max 3 mm

- Deviation layer surface from

regulated height		 	       max>3mm

- Deviation from demanded

Side fall 				      max>0,2%.

Execution technology

Base preparation

Asphalt layer can be placed on a base which is dry and which in any case isn’t frozen.

Before work start surface has to be well cleaned with steel brushes and blown with compressor. After finishing surface cleanup, Supervisor will record vertical alignment and surface flatness.

On parts where layer surface is making deviation from regulated height for more than +15m

It’s necessary for contractor do correction of surface according to demands required by project solution, regarding:

- On places where base surface is under regulated vertical alignment should do correction by increasing layer of asphalt mixture with asphalt concrete – wearing course,

- On places where base surface is above regulated vertical alignment should take extra asphalt mass in surface by rototillings.

Preparing and transport of asphalt mixture

Asphalt mixture has to posses griddle with 16mm whit will be removed unapproved grain size in mineral mixture.

Bitumen temperature needs to be between 150-165°C.

Aggregate temperature mustn’t be higher than bitumen temperature for 15°C.

Temperature of asphalt mixture in mixer should to be between limits 150-170°C.(exceptionally 175°C).

Asphalt mixture placing

Asphalt temperature mixture on place of placing mustn’t be lower than 140°C and higher than 175°C.

Period of work execution

Wearing course with specification from these technical conditions can be placed exceptionally in period from 15th of April until 15th of October, regarding in period when air temperature is higher than 5°C, without wind or min 10°C with a wind. Placing asphalt mixture mustn’t be done when there is mist or when it’s raining. Surface temperature mustn’t be lower than +5°C.

Quality control

Previous tests of asphalt mixture

Before work start contractor is obligated to make a project of previous asphalt mixture in authorized laboratory agreement with all demands of this technical conditions.

None work mustn’t start until contractor doesn’t suggest previous mixture on agreement to Supervisor. Certificates base materials and previous mixture mustn’t be older than 6 months. In case that there are some changes in base materials or it’s changed choice of materials, Contractor’s duty is to suggest to Supervisor in written note suggestion for change of adopted asphalt mixture regarding to suggest new previous mixture on agreement, before start using those materials.

Proven work composition of asphalt mixture

Quality of previous asphalt mixture is proving with test work with the fact to do asphalt mixture accepted at the very factory, and placing quality on test area. If quality of base materials on construction site doesn’t match this technical conditions. Contractor’s duty is to provide new quality base materials. If dozing with base materials, according to previous mixture, can’t satisfy all regulated demands for physical- mechanical characteristics of asphalt mixture and for placed layer, it is necessary to do correction of dozing base materials and repeat test work. Just after test work achieves all wanted demands, Supervisor will adopt work mixture and give agreement for non-stop work. Proven work composition of asphalt mixture is being done by authorized laboratory.

Quality control

For providing regulated quality in building process Investor or laboratory engaged from his side will do regular control tests, those are:

Bitumen testing

Contractor can get bitumen only under condition that for every delivery provide manufacturer certificate which will be delivered to Supervisor, regarding to laboratory.

Beside insight in manufacturer’s certificate, operational laboratory will execute and regular tests in short notice (,,PK”, penetration and breaking point) which is at the:

- Work start,and

- On each 100t of crushed filer

Testing of physical-mechanical compositions of asphalt mixture and placed layer

These tests will execute operational laboratory:

- At the start of work

- On each 2000m2.

Sample of asphalt mass is being taken for hot just laid out mixture behind finisher. Compressibility control and cavities in road is being done by taking out from upper construction, on the same place where sample from hot asphalt mixture was taken.

GENERAL CONDITIONS FOR WORK EXECUTION

General notice

Do work by instruction of Supervisor without who is not allowed to make any changes, or executing significant stages.

Unit prices of all work positions in Bill of Quantities are final prices of Contractor and those are including next:

- All necessary preparations and final work which are providing quality and whole job done.

- All cost necessary for executing work itself and exactly for: material, tools, scafell, directed costs, montage and transportation and all expenditure such as taxes and contributions according to valid laws for prices structure.

All work has to be completely done as predicted by project and drawings, done right according to technical conditions and standards with quality materials and experts according to conditions of authorized interested communal and other firms.

For all materials, semi-finished and done products which are being used on this type of work, Contractor’s duty is to bring samples to Supervisor on approving, regarding to do systematic testing and that about that testing bring valid evidence to Supervisor or to Purchaser. This testing are falling on Contractor’s budget.

Material which is not appropriate to technical regulative, conditions and standards mustn’t be used, and Contractor’s duty is to remove it from construction site without wage.

If technical documentation isn’t complete or incorrect, Contractor is obligated to ask in short notice amendment for it and all necessary interpretation. Eventually necessary demolitions of already done sections of object which are consequence of mistake not reading documentation enough goes on Contractor’s  budget without any rights for cost wage and deadline extension.

Contractor is obligated that all measures in design control on site.

Contractor is obligated that on construction site close and compress all pits, holes and around construction which he had to make during work, to even and clean, to handover cleaned from waste, during the work and until handover maintain order on construction site.

This entire works need to be calculated in price of right positions and will not be paid separately.

Contractor is obligated to keep all done work safe until handover and in that purpose do necessary security by instruction of Supervisor which is pre-calculated in unit price and not will be paid separately.

Bill of Work of done work will be done according to arrangement documents and according to construction book will be notarized from Supervisor. If Contractor without agreement of Investor during construction work back off from dimensions predicted  by project documentation, all consequences  bounded with that go on budget of contractor.

Preparation work

General description

Contractor’s is obligated before work start, to according to project design and prepared terrain record cross sections and about eventually disagreement notifies supervising service which will ascertain that.

For case that contractor doesn’t do by before mentioned, it is considering that he given terrain profiles accepting as valid. Before work start contractor is obligated according to design mark paths, calm rests, sport terrains and kids playgrounds with chainage peg, so that in each faze marked surface be easily seeable.

Markers have to be kept from destruction, and eventually destroyed have to be placed again. Bill of Quantities and payment is being done by m2 marked surface together with recorded profiles.

On is which contains soil work it’s needed to cut all vegetation predicted for removing, stumps take out and remove (put on a landfill) out of range which is work included. Trees that were cut put BoQ with calculation per piece and shrub and rest of vegetation calculate per m2.