# VOLUME 3

# TECHNICAL SPECIFICATIONS

- Preliminary works

- 1.01  STAKING OUT AND MARKING OF THE ROUTE AND STRUCTURES

Prior to the beginning of the works, Contractor shall perform the required marking of the center lines of the roads, intersections and structures. Marking shall be performed pursuant to the marking plan stated in the design. During the works, traverse points, benchmarks and control points. If the design does not provide data on traverse points and benchmarks, they shall be obtained from the relevant company for independent staking out.

Calculation of the performed works shall be made pursuant to the linear meters of the staked out route.

1.02	CUTTING OF THE BUSH

On the width of the road reserve intended for the construction of the road base, bush shall be cut. The cut bush shall be categorized, stacked into figures and stored on adequate place for loading and transportation where it will not disturb the execution of the works. The location for storage shall be determined in accordance with the supervisor.

Calculation of the works shall be made pursuant to the square meter of the overgrown surface of land from which the bush has been removed, for all the work, material and transportation, pursuant to the abovementioned description.

- 1.03  CUTTING OF THE TREES

On the width of the road reserve intended for the construction of the road base, trees shall be cut. Notching of a tree shall be performed mechanically at the height of up to 80 cm above the ground and the notched tree shall be carefully felled. Afterwards, branches shall be pruned, wood mass shall be classified and prepared for the transportation. Storage location shall be determined in accordance with the supervisor. During the works, protection measures shall be taken in order to avoid potential damages to the surrounding structures and property in general.

Calculation of the works shall be made pursuant to the number of felled trees for all the work, material and transportation, pursuant to the abovementioned description and trunk diameters.

- 1.04  REMOVAL OF THE STUMPS AND ROOTS

On the width of the road reserve intended for the construction of the road base, stumps of the felled trees and the found ones shall be removed. Stumps shall be excavated mechanically. Obtained wood mass shall be classified, loaded into the means of transport, transported to the storage the location of which shall be determined by the supervisor.

Calculation of the works shall be made pursuant to the number of removed stumps for all the work, material and transportation, pursuant to the abovementioned description.

- 1.05 EXCAVATION FOR DETERMINING THE POSITION OF UNDERGROUND INSTALLATIONS

This work covers manual excavations which are foreseen in the design or by the supervisor’s request for the needs of cutting grips and consequently the determination of the position of installations. 95% of the excavation is foreseen to be done manually and 5% mechanically. Excavated soil material shall be stacked into shapes suitable for loading.

Calculation of the works shall be made pursuant to the cubic meter of the excavated uncultivated material with the pushing of up to 20 m, of the prepared soil material for the transportation.

- 1.06  DEMOLITION OF THE CURBS

Existing curbs, regardless of the type, which are to be removed according to the design, shall be demolished manually together with the concrete base below the curb. Demolished curbs shall be cleared off from concrete and plaster, loaded into the vehicle, transported to the storage, unloaded and stacked into regular shapes. Debris remaining after the demolition of curbs shall also be loaded onto the vehicle and transported to the storage the location of which shall be determined by the supervisor, unloaded and rearranged on the storage.

If the demolished curbs can be reused, they shall be deported to the new location for placement.

Calculation of the works shall be made pursuant to the linear meter of the removed curb, for all the work, material and transportation, pursuant to the abovementioned description.

- 1.07 DEMOLITION OF SIDEWALKS AND CYCLE LANES

Sidewalks and cycle lanes which are to be removed by the design shall be demolished. Average thickness of the base is 30-40 cm, of various composition. If the pavement is composed of the paving slabs, these slabs shall be taken out manually, cleaned and loaded onto the vehicle. Debris remaining after the demolition shall be loaded onto the vehicle and transported to the storage the location of which shall be determined by the supervisor, unloaded and rearranged.

Calculation of the works shall be made pursuant to the square meter of the demolished pavement or cycle lane for all the work, material and transportation, pursuant to the abovementioned description.

- 1.08  DEMOLITION OF OTHER TRAFFIC AREAS

Concrete plateaus and road accesses shall be demolished as foreseen, regardless of their purpose, which are to be removed from the design or adapted to the road rehabilitation design. Average base thickness is 30-40 cm. If the traffic surface consists of slabs, they shall be taken out, manually cleaned and stacked aside. Debris remaining after the demolition shall be loaded onto the vehicle and transported to the storage according to the supervisor’s instructions, unloaded and rearranged.

Calculation of the works shall be made pursuant to the square meter of the demolished parking space, for all the work, material and transportation, pursuant to the abovementioned description.

1.09 PREPARATION OF THE OPERATIVE JOINTS FOR THE CONTINUATION OF ASPHALT WORKS

On the segments where the existing asphalt pavement is to be expanded or continued pursuant to the design, staggered notching of asphalt pavement (d=6-10 cm) with pneumatic drill equipped with excavation blade or circular cutter. Notching line on pavement surface shall be straight. The height of notching levels are equal to the height of the executed layers, with horizontal moving of about 10 cm for asphalt layers. Material obtained from the demolition shall be loaded onto the vehicle, transported to the storage or used on the site.

Calculation of the works shall be made pursuant to the linear meter of the prepared pavement for the continuation pursuant to the abovementioned description.

- 1.10 DISLOCATION OF THE EXISTING UNDERGROUND INSTALLATIONS

The dislocation shall be carried out fully pursuant to the separate design or the instructions of the owner of installations and the supervisor as well as the regulations covering such type of installations.

Calculation of the works shall be made pursuant to the piece of dislocated installation (according to the subcontractor’s bid, which shall be inserted in the bill of quantities when preparing the bid).

- 1.11 PRESERVATION OF THE EXISTING UNDERGROUND INSTALLATIONS

Plastic or concrete cable ducts or connectable cable ducts shall be laid on the planned and compacted surface of the trench or the position and the height of the elements shall be checked so that they could be inserted at a later point in time, and the trench shall be refilled with soil while the layers shall be compacted.

Calculation of the works shall be made pursuant to the linear meter for all the work and material, depending on the type of cable duct - connectable cable duct.

- 1.12 DISLOCATION OF THE OVERHEAD TC LINES

The dislocation shall be carried out fully pursuant to the separate design or the instructions of the owner of underground or overhead TC installations and the supervisor as well as the regulations covering such type of installations.

Calculation of the works shall be made pursuant to the piece of dislocated TC installation (as lump sum, pursuant to the subcontractor’s bid, which shall be inserted in the bill of quantities when preparing the bid).

- 1.13 LEVELLING OF THE EXISTING MANHOLES

Existing sewage manholes, gullies and pipeline holes, which do not match the new levels in the design with their height, shall be fitted in with adequate lifting-lowering (10-20 cm) of the iron rim, accompanied by the demolition and construction of a concrete cushion below the rim. All the material originating from this work shall be loaded into the vehicle, transported to the storage as instructed by the supervisor, unloaded and rearranged.

Calculation of the works shall be made pursuant to the piece of the regulated manhole and gulley, for all the work and material, pursuant to the abovementioned description.

1.15 ARCHAEOLOGICAL SUPERVISION FOR MONITORING EARTH WORKS

Pursuant to the decision issued by the Subotica Cultural Heritage Bureau, during the soil excavations deeper than 15 cm below the surface layer, archaeological supervision of earth works on the road route shall be provided. This item covers all costs for engaging one archaeologist and one technician as well as all accompanying costs for their supervision.

Calculation of the works shall be made as lump sum, pursuant to the bid submitted by the Subotica Cultural Heritage Bureau for all the work and material, pursuant to the abovementioned description.

- 2. EARTHWORKS

- 2.01 EXCAVATION OF HUMUS

Excavation of humus shall be performed 95 % mechanically and 5% manually within the limits of designed thickness and width under-above road base – street. The excavation of humus shall be performed only after completed marking of designed width, slope gradient and surveillance of terrain in terms of cross-sections. Thickness of humus layer which is being removed is typically defined in the design based on geomechanical testing, but it can be also defined in-situ, together with the supervisory body, per profiles and road sections. In case that during construction the necessity of thickness alteration is detected, this alteration shall be recorded in construction log book by the supervisory body.  Pushing humus away shall be performed in such a manner so that it is not mixed with soil for embankment, and that the drainage of road base is enabled. Excavated humus in quantities sufficient for topsoiling of green areas, shoulders and slopes shall be stored in a shape of regular stock piles, and the rest shall be prepared for transportation.

Calculation of executed works is performed per cubic meter of removed uncultivated soil with pushing away up to 10 m, for cumulative works and material.

- 2.02 WIDE EXCAVATION BY BUCKET-WHEEL EXCAVATOR

This performance covers wide excavations which may be carried out only by a bucket-wheel excavator in a relatively narrow areas which are specified in the design or defined by a request of the supervisory body: in cuttings, side cuts, borrow-pits and larger deviations. Excavation shall be performed as wide digging as regards designed ground levels and grade in relation to cross-sections. Before the excavation starts, outstanding markings of cross-sections shall be checked. It is foreseen that 80% of excavation shall be performed mechanically and 20% manually. Excavated earth material shall be stored and loaded.

Calculation of executed works is performed per cubic meter of excavated uncultivated material from the stored or loaded one.

- 2.03 COMPACTING OF SUB-SOIL

Upon excavation of humus, compacting of sub-soil is performed under the embankment and dug side-cuts. The compacting of sub-soil shall be performed by mechanical means. It is required to compact the subsoil in accordance with the standard Proctor method 100% of the maximum laboratory compactness, and in depth up to d=50 cm. In case the required compactness cannot be achieved at certain places, compacting process shall continue by adding sand-gravel material until required values of compactness are reached. This additional work shall not be paid separately, but only costs of procurement of sand-gravel material.

Calculation of executed works is performed per cubic meter of compacted sub-soil for cumulative work, material and control tests.

- 2.04 CONSTRUCTION OF SAND EMBANKMENT

Process of construction the sand embankment calls for procurement of sand with transportation, filling, spreading, necessary moistening, planning, and compacting according to the regulations and control tests. Construction of embankment is performed according to the designed cross-sections, ground levels and gradients as provided for in the design with permitted tolerances of 5 cm. Embankment shall be constructed in horizontal layers up to 30cm thick. Compacting of embankment shall be performed by vibrational devices with compacting until the required level of compactness is achieved.  Quantities estimated for construction of embankment shall include a part of embankment under the shoulders. Compactness test of constructed layers shall be carried out by test circular plate with a diameter d=30 cm, requiring a minimum value of modulus of compressibility Ms=25 MN/m2.

Calculation of executed works is performed per cubic meter of compacted sub-soil for cumulative work, material, transport and control test in accordance with the description given above.

2.05 CONSTRUCTION OF EMBANKMENT MADE FROM SOIL MATERIALS

The work on construction of soil embankment includes filling with soil from cuttings or transported from borrow-pits, spreading, necessary moistening or drying, planning, compacting as provided for in regulations and control tests. Construction of embankment shall be carried out according to the designed cross-sections, ground levels and gradients as provided for in the design with permitted tolerances of 5 cm. Embankment shall be constructed in horizontal layers up to 30cm thick, with the drainage gradient. Compacting of embankment shall be performed by vibrational means or static roller, with compacting until the required level of compactness is achieved. Quantities estimated for construction of embankment shall include a part of embankment under the shoulders. Compactness test of constructed layers shall be carried out by test circular plate with a diameter d=30 cm, requiring a minimum value of modulus of compressibility Ms=25 MN/m2.

Calculation of executed works is performed per cubic meter of compacted sub-soil for cumulative work, material, transport and control test in accordance with the description given above.

- 2.06 PLANNING AND ROLLING OF SUBGRADE

Subgrade treatment includes subgrade planning according to the designed ground levels and additional compacting on the entire width of formation until the required level of compactness is achieved. Final rolling shall be performed by smooth roller in order to reach flat surface of subgrade, while the tolerances of (+,-) 2 cm in relation to the designed ground levels are permitted. Subgrade compactness test shall be carried out by test circular plate with a diameter d=30 cm, requiring a minimum value of modulus of compressibility Ms=25 MN/m2.

Calculation of executed works is performed per cubic meter for cumulative work and material, with control tests.

- 2.07 TOPSOILING OF FLAT AND TILTED EMBANKMENT SURFACES

The works includes topsoil of flat surfaces, cutting slopes and embankments and shoulders, with necessary grassing, in layers up to 15 - 30 cm. Topsoiling of surfaces shall be performed by humus which has been previously removed from the alignment and stored in stock piles. If the stored humus is dry, it shall be spread and moistened when applied.  Upon spreading and planning of humus layer, it should be easily compacted. In case there isn’t enough humus in-situ, it should be obtained from the borrow-pit or from the place designated by the supervisory body. Delivery of material is separately calculated per item defining transport of soil materials.

Calculation of executed works is performed per square meter of topsoiled and grassed surface, and production cost covers a total of all works and material.

- 2.08 SPREADING OF SOIL MATERIAL ON LANDFILL

Humus surplus and excavated soil material up to the category according to which it has been transported to the landfill shall be spread in layers at the landfill and roughly planned in accordance with the instructions provided by the supervisory body.

Calculation of executed works is performed per cubic meter of uncultivated spread material, for all works and material cumulatively.

- 2.09 TRANSPORT OF SOIL MATERIAL

Humus surplus and excavated soil material, along with the supply of material from borrow-pits for construction of embankments or topsoiling until certain category is reached, shall be loaded and transported to landfill or the place of incorporation, as per distances given in the Bill of Quantities. This item includes loading into vehicles, transportation, unloading and rough spreading.

Calculation of executed works is performed per cubic meter of loaded, transported, unloaded and roughly spread uncultivated material.

3. PAVEMENT STRUCTURE

3.01 CONSTRUCTION OF THE LOAD-BEARING LAYER FROM MECHANICALLY COMPACTED GRAINED ROCK MATERIAL 0/31.5 mm

The work involves the procurement and installation of granular rock material in the load-bearing layer of the pavement structure. Works can only begin when the supervisor accept a subgrade regarding evenness, designed levels and slopes, and compactness. Materials for the production of a load-bearing layer can be: natural gravel, crushed stone material, a mixture of natural gravel and crushed material and mixture made up of several fractions. All of the above materials must meet certain conditions regarding mechanical characteristics, granulometric composition, bearing capacity and other states according to the applicable standards.

On the planned and rolled subgrade, grained stone material is applied, it is spread by a grader or other suitable means, it is wetted and compacted to the required compactness by suitable static and vibratory means. The load-bearing layer is carried out in layers of thickness from 20 to 40 cm, which is determined by design. The material must also meet the requirements for resistance to frost. The upper surface of the load-bearing layer should be made according to the designed levels and slopes, while the evenness of the finished layer is controlled by a rod of length L = 4m, and the allowed deviation is (+, -) 1cm. The inspection tests regarding compactness should be carried out with a circular plate of diameter d = 30 cm, and the smallest modulus of compressibility depends on the type of stone material:

for natural gravel                                                                         Me = 50 MN / m2.

for a mixture of natural gravel and crushed material                   Me = 60 MN / m2.

for crushed stone material                                                          Me = 70 MN / m2.

Calculation of executed works is carried out per cubic meter of the finished load-bearing layer from mechanically compacted grained material, for all work, material, procurement and transport of stone material and control tests.

3.02 CONSTRUCTION OF BITUMENIZED LOAD-BEARING LAYER (BBL22A)

The upper bituminous load-bearing layer (BBL) is a bearing layer in a pavement structure, made of a mixture of stone material, rock flour, and bitumen as a binder. By the grain size, it is classified as BBL 22, BBL 32 and BBL 45.

According to the type of stone used, depending on the design and the designed load capacity, it is divided into:

BBL A, made by crushed separated stone material according to JUS B.B3.100 (stone aggregate), with the addition of rock flour as needed;

BBL B, produced by crushed separated rock material with at least three fractions and a maximum grain of 45 mm, with the addition of rock flour as needed;

BBL C, made of unseparated crushed rock material with correction by the addition of rock material, or unseparated natural unbound material with addition of at least 30% of the stone mixture of crushed grain above 4 mm and up to 45 mm, with correction by the addition of sand or rock flour; BBL D, made of unseparated natural unbound material with the largest grain size of 45 mm, with revision of the composition by adding sand or rock flour.

Rock material, sand, and rock flour must satisfy the conditions prescribed by YUS. There must be no organic matter in the mineral mixture. The granulometric composition of the mixture must be such that it meets the prescribed screening curves from the standard.

Bitumens BIT 60 and BIT 90 are used as a binder. The exact share of bitumen is determined by making the first mixing mixture and approximately is of 3.3-5.2% depending on the type.

Before the start of the work, all material to be used must be subjected to a laboratory examination, which must be by the technical conditions for the preparation of the bedding YUS.U.E9.020. Preparation of the mass is done with modern asphalt bases and incorporation with finishers with necessary rolling by combined rubber and smooth rollers. Transport the mass by vehicles - tipper trucks. During the preparation and placing of the mass, all control tests, material testing and asphalt mass must be carried out following the standards.

Layers must be carried out in designed thicknesses and designed cross-fall.

Control tests of the produced asphalt mass are made for every 1500 tons of mass produced, namely: fraction of bitumen, granulometric composition, stability, stability and deformation ratio, cavity share and bitumen content of the cavity. Inspection tests of the embedded layer are carried out on every 2,000 m2 of the layer, namely: the percentage of the cavities, the degree of compactness and the thickness of the layer.

Calculation of executed works is performed in square meters of the upper surface of the actual made layer. The price includes all costs of purchasing materials, production, and incorporation of asphalt mass, transport, equipment, preliminary and control tests and all other costs necessary for the execution of works. Exceptionally, at leveling of the existing surface of the carriageway during the reconstruction of the traffic surfaces, the calculation can also be done per tonne or m3 of built-in mass.

3.03 PREPARATION OF WEARING COURSE-ASPHALT CONCRETE (AC11)

The wearing course from the asphalt concrete is made from the mixture of crushed rock material, rock flour, and bitumen as a binder. According to nominal grain size, it is classified as: AC 4, AC 8, AC 11, AC 16 and AC 22.

According to granulometry composition of rock mixture the asphalt concretes are classified as :

Wearing course of a broader granulometric composition of rock mixture AC 4 - AC 16

Wearing course of narrower limit the range of rock mixture granulometric composition AC11s – AC22s.

Rock material, sand and stone flour must satisfy the conditions prescribed by YUS. For roads with heavy traffic loads, rock material must be of eruptive origin. There must be no organic matter in the mineral mixture. The granulometric composition of the mixture must be such that it satisfies the prescribed screening curves from the standard.

Bitumen BIT 60 and BIT 90 are used as binder and for close-grained asphalt concrete AC4 and AC11 and bitumen BIT 130. The correct bitumen content is determined by the preparation of the mixture with the previous composition, and it is approximately 4.5 to 8.0%, depending on the type of asphalt concrete.

Before the commencement of the work, all material to be used must be laboratory tested and must be following the technical conditions for the preparation of asphalt concrete. Preparation of the mass is done with modern asphalt bases, and placing with finishing machines with the necessary rolling with combined rubber-tired and smooth-wheel rollers. Transportation of the mass is carried out with vehicles – tipper trucks. In the course of preparing and incorporation of the mass, all control tests, material testing, and asphalt mass testing must be carried out following the standards.

Layers must be carried out in designed thicknesses and designed crossfalls, on clean bedding. Control tests of the produced asphalt mass are carried out for every 500 tons of mass produced (5,000 m2) for heavy-duty roads and 600 tons (6,000 m2) for other roads, as follows: bitumen content, granulometric composition, stability, stability and deformation ratio, cavity share and cavity fulfillment with bitumen. Inspection tests of the embedded layer are carried out on every 2,000 m2 of the made layer: the cavity share, the degree of compactness and the thickness of the layer.

Calculation of executed works is performed in square meters of the upper surface of the actual prepared layer. The price includes all costs of purchasing materials, production, and incorporation of asphalt mass, transport, equipment, preliminary and control tests and all other costs necessary for the execution of works.

3.04 CONSTRUCTION OF A SURFACING FROM CONCRETE

Above the properly executed and accepted bedding, make a concrete surfacing in the layer of designed thickness. As the aggregate, use permanent natural river gravel and sand or crushed material, and these must meet the technical requirements for the rock aggregate YUS B.B3.050. For the manufacture of concrete only use cement PC 350 according to YUS B.C1, and the concrete water must be clean and pre-tested. Concrete must be prepared by machine, whereby the weight dosage of individual components must be ensured. The concrete mixture is transported to the place of incorporation with means of transport where the segregation process is not possible. Through a finely-planned, well-compacted and received bedding, lay a kraft paper so that the individual strips overlap at least 5 cm in the direction of the crossfall. Incorporation of the concrete mass must be done by machine, high-frequency vibrating finisher. In the case of double layers, layers are usually made from the concrete of different qualities. The top layer should not be thinner than 5 cm. After execution of concreting, process crosswise and longitudinal joints. The width of the transversal joints should be 14-18 mm, and the longitudinal 20 mm. The concrete pavement must be protected against drying by wind and sun, and from moistening due to rain. After the carriageway is completed, there must be no traffic for seven days, and the filling of the joints with the YUS N.M3.095 sealing compound must be carried out only after the carriageway has completely solidified. During the construction of the concrete surfacing for all previous tests, the tests during construction and the finished pavement are subject to the technical conditions of YUS U.E3.020.

Calculation of completed works is done per square meter of concrete pavement constructed for all work and material with necessary testing and other costs.

3.05 LAYING OF CONCRETE CURBS

The work includes laying of concrete curbs of the most common dimensions 18/24, 12/18 and 6/20. The curbs are laid on a prepared concrete bedding of MB 20, and according to the design. Some details about the excavation, concrete base, laying of concrete, joints pointing and the rest should be done according to the details from the design. Sealing of 1 cm thick joints execute with cement mortar, which is made in a 1: 3 ratio. The height and layout position of the curb must be following the design. The curbs must be MB 40 and have the attestations of the required quality. Only healthy and undamaged curbs can be incorporated.

Calculation of completed works is done per meter of the laid curb, for all work and material, including the purchase and transport of curbs.

1. DRAINAGE

4.01 PREPARATION OF INFLOW-DISCHARGE CHANNELS

After marking the position of the inflow-discharge structure of the channels, and according to the design attachment, it should be made from the dense concrete MB 20 and place the lid. Material for the construction of this building as well as the way of incorporation should be following the applicable technical regulations and standards.

The calculation of the performed works is done according to a piece of the inflow-discharge building. The price includes all works and costs related to procurement and control.

4.02  PREPARATION OF PIPE CULVERT

According to the details and type of the design, execute a pipe culvert from finished concrete pipes with the head at the entrance and exit. For the tube, body use centrifuged prefabricated concrete pipes with laying on a padstone. All embedded material should comply with applicable YUS standards for this type of works. When performing the works, respect the conditions of the environment and in the case of excavation, apply the appropriate method of building the foundation pit.

The calculation of the performed works is done according to the linear meter of the constructed culvert, and according to the details from the design. The cost of production includes the costs of carrying out the works and the procurement of materials.

8.1  DESIGN OF TRAFFIC AND TRAFFIC SIGN WORK

Technical conditions for the execution of works are harmonized in all with the Rulebook on traffic sign work and specification of works for this design. The position numbers in the technical conditions for performance are in line with the position numbers in the Traffic sign work Rulebook.

The contractor must submit the appropriate documentation to the supervisory authority: the quality certificate of the foil classes 1 and 2 and 3, the certificate of quality of the traffic sign board and their conformity with the standard SRPS EN 12899 (Official Gazette RS No. 85/2017, Article 16 minimum conditions):

1. Class-based safety factor (PAF1)

2. Wind pressure class (WL5)

3. Dynamic snow pressure class (DSL1)

4. The largest temporary deflection class (TDB4), issued by an accredited laboratory.

Traffic signaling must be produced in accordance with Technical Instructions Nos. BS-02/2013 and BS-03/2013.

Elements of traffic signaling, covered by this design are:

1. TRAFFIC SIGNS

2. MARKINGS ON THE ROAD

6. TRAFFIC SIGNALS ON THE ROAD

7. ROAD EQUIPMENT

8. TECHNICAL FACILITIES FOR TRAFFIC DECELERATION

9. OTHER ROAD EQUIPMENT AND SIGNALLING

10. OTHER WORKS

❖ The technical conditions for the design, procurement, and incorporation of certain elements of traffic sign work are explained through individual positions of these works.

❖ The ordering of traffic signaling elements is done by design specifications.

❖ Development of different elements is done by European regulations, SRPS standards, Rulebook on traffic signaling ("Official Gazette of the Republic of Serbia" No. 85/2017, from now on referred to as the Rulebook) as well as detailed drawings in the design. In the process of traffic signs manufacture, the producers thereof shall comply with the provisions of the Technical Instructions (with binding application) on the manner of testing and the procedure for assessing the conformity of traffic signs on the state roads of the Republic of Serbia with the requirements of the standards, issued and adopted by JP "Putevi Srbije", Belgrade.

❖ Traffic sign background requirements: for all traffic signs including constructive reinforcements, the traffic sign background must be painted in gray tone in accordance with RAL 7043, with a minimum thickness of 12 μm (in accordance with EN 13523-1).

❖ Traffic sign construction requirements: traffic signs with an area not exceeding 1.1 m2 must be made from one part. Traffic signs whose surface exceeds 1.1 m2 are allowed to work from parts, with the necessary constructive reinforcement on the back of the sign.

❖ The placement or implementation of certain elements of traffic signaling is done on the basis of the situational solution, cross-sectional profiles and other drawings from the design, as well as on the basis of the Traffic Signaling Regulation and SRPS standards.

- TRAFFIC SIGNS

Traffic signs are made from materials and in the manner prescribed by the Rulebook. The standard traffic signs are made of the following materials:

1. Galvanized steel sheet with a bent edge (shortened GSSBE),

2. An aluminum sheet (abbreviated AS),

3. Aluminum sheet reinforced with clip (shortened ASC),

4. Aluminum sheet with a bent edge (shortened ASBE).

For the production of traffic signs, the use of aluminum materials with a tensile strength of minimum 155 N / mm2 for bent edges traffic signs and in an extruded aluminum profile (clips), i.e., minimum 200 N / mm2 for even signs, is permitted.

Materials used under DIN EN 573-1 and 573-2, or materials with the following markings, shall be used:

- EN AW 52 51 H 24 / H 34,

- EN AW 30 05 H 22 / H 49,

- EN AW 57 54 H 22 / H 34 / H 42.

The aluminum materials for the manufacture of sign parts assemblies and extruded components under DIN EN 573-3, or materials with the following labels, can be used:

- EN AW 60 60 T 4 / T 66,

- EN AW 60 05 A / T 6.

The face side of the sign, with all the symbols, letters and figures according to Article 14 of the Traffic Signaling Rulebook, must have reflective properties as follows:

1) Highway: signs that are placed next to a carriageway are made of materials of at least class 2 if there is no public lighting, from class 3 material, signs of traffic guidance are produced if public lighting exists, and the signs that are placed on the portals are made of materials class 3;

2) motor road: the signs that are placed next to the carriageway are made of materials of at least class 2, and on the portals of the material of class 3;

3) other state and claimed roads: signs are made from materials of class 2;

4) streets: signs are made of class 1 material.

Exceptionally from paragraph 1 of Article 14:

1) on the highway and motorway, the signs along the objects on the road: III-58, III-59, III-60, III-61, III-90, III-90.1, shall be made up of the materials of class 2  ;

2) on the other roads, except on the streets, from the materials of Class 3, the following signs are produced: I-32, I-33, I-34, I-34.1, I-35, II-1, II-2, III- III-6, III-7;

3) in the streets from the Class 2 material, the following signs shall be made: I-32, I-33, I-34, I-34.1, I-35, II-1, II-2, III-5, III- 7;

4) from the materials of Class 3, the following signs are produced: III-11, III-28, III-85, III-86, III-89, III-89.1, III-89.2;

5) from Class 1 material, the following signs are produced: II-40, II-41, II-41.1, II-42, III-19 III-20, III-21, III-22, III-98, and III-99.

Since the subject of processing are sections in the settlements and traffic nodes of the reference system on the state road, the design envisages the setting of standard traffic signs for this road category following the Traffic Signalling Rulebook, Technical Recommendation, and SRPS standard. Based on the mentioned above traffic signs have the following sizes:

1.1 Warning signs:

- Triangular with a length of side 90 cm;

- Rectangular: 120x60 cm;

- Rectangular: 30x100 cm;

1.2 Signs giving orders:

- Triangular with a length of side 90 cm;

- Circle with diameter Ø 60 cm;

- Circle with diameter Ø 40 cm;

1.3 Information signs:

- Square, side 60 cm;

- Square, side 50 cm;

- Rectangular: 60x90 cm;

- Rectangular: 80x60 cm;

- Rectangular: 35x30 cm;

- Circle diameter Ø 60 cm;

1.4 Supplementary boards:

- Square, side 60 cm;

- Rectangular: 60x30 cm.

On a fluorescent base:

- Rectangular: 120x140 cm.

Traffic signs next to the road outside the settlement, are set at the height of 1.20 to 1.40 m.

Traffic signs next to the road are located at intersections in the settlement, outside pedestrian areas, depending on the number of signs, at the height of 1.4m to 1.8m, and on pedestrian surfaces at the height of 2.2m to 2.4m.

The set signs must be secured from turning and shearing.

The set signs must be maintained regularly.

The signs are set so that their plane deviates from the horizontal by 3 to 5º in the field from the normal on the axis of the road.

The design determines the placement of the sign in the cross profile design.

Traffic signs are placed on the post next to the carriageway on the right side, in the direction of movement.

The height is calculated from the surface of the carriageway to the lower edge of the traffic sign.

Exceptionally, at the height of 1.4m, the signs II-45 (keep right), II-45.1 (keep left) and II-45.3 (keep either side) are placed.

Exceptionally, at the height of 0.8m signs are set: I-35 (approaching the level crossing with barrier or gate), III-98 (kilometer peg) and III-99 (number of road, number of road section and mileage).

Exceptionally, at the height of 0.5m, the signs are set: III-84 and III-84.1 (the sign board for the top of the division island).

The distance between the edge of the carriageway and the most extended edge of the traffic sign, which is placed on the road, intersections and in the settlement, outside the pedestrian area, is between 0.75 and 1.50 m. It is exceptionally 0.5m if there is a protective fence and if the traffic profile contains stoppages.

The disintegration between the edge of the carriageway and the most extended edge of the traffic sign placed on pedestrian surfaces is from 0.30 m to 1.5 m.

The manufacturer must guarantee the unchangeable quality of the sign for at least five years from the date of installation, or 7 years from the date of manufacture.

The manufacturer is obliged to print on the back of the sign the code of the sign from the design, and in the case of placement of the envelope, the code of sign must also be located on it.

QUALITY CONTROL

The manufacturer must possess a certificate for all materials used in the production of standard traffic signs. Quality control is performed in accordance with SRPS Z.S2.300.

CALCULATION OF WORKS

The price of the traffic sign includes the purchase, delivery, and transport to the contracted place of delivery according to the request of the contractor, all mounting elements for fixing on the carrier (reinforcement, clamps, cuffs, screws, etc.), as well as quality control.

A piece of the traffic sign does the calculation for each type of work.

1.3.2 Information signs for traffic control

The position includes the manufacture, procurement, and installation of information signs for traffic control (signs manufactured according to the drawings in the design).

Information signs for traffic control shall be designed in accordance with the Traffic Signaling  Rulebook ("Official Gazette of the Republic of Serbia" No. 85/2017) and Serbian traffic signaling standards in the zone of the intersection SRPS Z.S2.313, SRPS Z.S2 .314, SRPS Z.S2.316, SRPS Z.S2.317, SRPS Z.S2.317 / 1 and SRPS Z.S2.319 of February 2014 as well as with the Law on Official Use of Languages ​​and Letters of the Republic of Serbia ("Official Gazette of the Republic of Serbia", No. 45/91, 53 / 93,67 / 93, 48/94, 101/2005) and the Decree on the categorization of state roads ("Official Gazette of RS", No. 105 and 119/2013)

Information signs for traffic management covered by this design are:

1.3.2.1 Intersection and roundabout,

The signs of larger dimensions must have appropriate reinforcements that ensure the compactness of its surface, in which case the sign is fastened to the carrier using it.

These reinforcements can only be on the back of the sign. There should be no fixings on the face of the sign (screws, bolts, etc.), as well as possibly joints of individual sheet plates, which would interfere with the readability and reflection of the sign, both in the daylight and in the lighting of the car's headlights.

The information signs of the intersection and the roundabout are placed on mountings consisting of one or more parallel vertical mountings, on particular constructions (trusses), or semi-portal mountings, as foreseen by design in situations.

The situated signs must be secured from turning and shearing.

The situated signs must be maintained regularly.

The signs are set so that their plane deviates from the horizontal by 3 to 5º in the field from the normal on the road axis.

The design determines the position of the sign in the cross profile design.

Traffic signs are placed on the post next to the carriageway on the right-hand side, in the direction of movement.

Traffic signs along the road are located at intersections in the settlement, outside pedestrian areas, depending on the number of signs, at the height of 1.4m to 1.8m, and on pedestrian surfaces at the height of 2.2m to 2.4m.

The height is calculated from the road surface to the lower edge of the traffic sign, i.e., mounting (semi-portals).

The distance between the edge of the carriageway and the most protruded edge of the traffic sign, which is located at the intersections and in the settlement, outside the pedestrian area, is between 0.75 and 1.50 m. It is exceptionally 0.5m if there is a protective fence and if the traffic profile contains stopping lanes.

The distance between the edge of the carriageway and the most protruded edge of the traffic sign placed on pedestrian surfaces is from 0.30 m to 1.5 m.

The manufacturer must guarantee the unchangeable quality of the sign for at least 5 years from the date of installation, or 7 years from the date of manufacture.

The manufacturer is obliged to print on the back of the sign the code of the sign from the design, and in the case of placement of the envelope, the code sign must also be located on it.

The face of information signs for vehicle lane changing must have reflective properties of the material (anti-graphite film) of Class 2.

      - Vehicle lane changing

The information signs for vehicle lane changing are placed on mountings consisting of one or more parallel vertical mountings, on particular constructions (trusses), or to semi-portal mountings, as foreseen by design in situations.

The situated signs must be secured from turning and shearing.

The situated signs must be maintained regularly.

The signs are set so that their plane deviates from the horizontal by 3 to 5º in the field from the normal on the road axis.

The design determines the position of the sign in the cross profile design.

Traffic signs are placed on the post next to the carriageway on the right side, in the direction of movement.

Traffic signs along the road are located at intersections in the settlement, outside pedestrian areas, depending on the number of signs, at the height of 1.4m to 1.8m, and on pedestrian surfaces at the height of 2.2m to 2.4m.

The height is calculated from the road surface to the lower edge of the traffic sign, i.e., mounting (semi-portal).

The distance between the edge of the carriageway and the most protruded edge of the traffic sign, which is located at the intersections and in the settlement, outside the pedestrian area, is between 0.75 and 1.50 m. It is exceptionally 0.5m if there is a protective fence and if the traffic profile contains stopping lanes.

The distance between the edge of the carriageway and the most protruded edge of the traffic sign placed on pedestrian surfaces is from 0.30 m to 1.5 m.

The manufacturer must guarantee the unchangeable quality of the sign for at least 5 years from the date of installation, or 7 years from the date of manufacture.

The manufacturer is obliged to print on the back of the sign the code of the sign from the design, and in the case of placement of the envelope, the sign code must also be located on it.

The face of the information signs for vehicle lane changing must have reflective properties of the Class 2 material (foil).

1.3.2.4 Arrow direction sign

The information signs for vehicle lane changing are placed on mountings consisting of one or more parallel vertical mountings, on particular constructions (trusses), or to semi-portal mountings, as foreseen by design in situations.

The signs must be secured from turning and shearing.

The situated signs must be maintained regularly.

The signs are set so that their plane deviates from the horizontal by 3 to 5º in the field from the normal on the road axis.

The design determines the position of the sign in the cross profile design.

Traffic signs are placed on the post next to the carriageway on the right side, in the direction of movement.

Traffic signs along the road are located at intersections in the settlement, outside pedestrian areas, depending on the number of signs, at the height of 1.4m to 1.8m, and on pedestrian surfaces at the height of 2.2m to 2.4m.

The height is calculated from the surface of the carriageway to the lower edge of the traffic sign.

The distance between the edge of the carriageway and the most forward edge of the traffic sign, which is located at the intersections and in the settlement, outside the pedestrian area, is between 0.75 and 1.50 m. It is exceptionally 0.5m if there is a protective fence and if the traffic profile contains stopping lanes.

The distance between the edge of the carriageway and the most forward edge of the traffic sign placed on pedestrian surfaces is from 0.30 m to 1.5 m.

The manufacturer must guarantee the unchangeable quality of the sign for at least 5 years from the date of installation, or 7 years from the date of manufacture.

The manufacturer is obliged to print on the back of the sign the code of the sign from the design, and in the case of placement of the envelope, the sign code must also be located on it.

The face of the information signs for vehicle lane changing must have reflective properties of the Class 2 material (foil).

1.3.2.5 Directional panel

The signs of larger dimensions must have appropriate reinforcements that ensure the compactness of its surface, in which case the sign is fastened to the mounting.

These reinforcements can only be on the back of the sign. There should be no fixings on the face of the sign (screws, bolts, etc.), as well as possibly joints of individual sheet plates, which would interfere with the readability and reflection of the sign, both in the daylight and in the lighting of the car's headlights.

The information signs for traffic management are placed on mountings consisting of one or more parallel vertical mountings, on particular constructions (trusses), or to semi-portal mountings, as foreseen by design in situations.

The information signs for traffic control are delivered together with the appropriate mountings, designed by the manufacturer of the sign.

The placed signs must be secured from turning and shearing.

The placed signs must be maintained regularly.

The signs are set so that their plane deviates from the horizontal by 3 to 5º in the field from the normal on the road axis.

The design determines the position of the sign in the cross profile design.

The traffic signs are placed on the post next to the carriageway on the right side, in the direction of movement.

Traffic signs along the road are located at intersections in the settlement, outside pedestrian areas, depending on the number of signs, at the height of 1.4m to 1.8m, and on pedestrian surfaces at the height of 2.2m to 2.4m.

The height is calculated from the surface of the carriageway to the lower edge of the traffic sign, i.e., mounting (semi-portal)

The distance between the edge of the pavement and the most protruded edge of the traffic sign, which is located at the intersections and in the settlement, outside the pedestrian area, is between 0.75 and 1.50 m. It is exceptionally 0.5m if there is a protective fence and if the traffic profile contains stopping lanes.

The distance between the edge of the carriageway and the most protruded edge of the traffic sign placed on pedestrian surfaces is from 0.30 m to 1.5 m.

The manufacturer must guarantee the unchangeable quality of the sign for at least 5 years from the date of installation, or 7 years from the date of manufacture.

The manufacturer is obliged to print on the back of the sign the code of the sign from the design, and in the case of placement of the envelope, the sign code must also be located on it.

The face of the information signs for traffic management, with all symbols, letters, and numerals, must have reflective properties of the Class 2 material (anti-graphite foil).

1.7 Placement of traffic signs on the posts mountings

By placing two signs on the same post, for the different directions, the back of the signs II-1 and II-2 must not be covered.

Mounting the sign on the built-in mounting (the price includes the transport of the sign and the workers from the point to the place of work, setting and fixing the sign on the post by tightening the clips and notching the nuts so that they can not easily be loosened. The purchase of the sign with transportation from the manufacturer to the point is not included in the price).

1.8 Mountings of traffic signs

The position includes the production, procurement, and installation of traffic signs:

1.8.1. Single post tubular mountings

- Post tubular mountings are made of a steel-drawn tube of uniform cross-section and thickness, depending on the number and type of signs that are placed on the mounting, which is indicated in the specifications, or the bill of quantities of the mountings in the design.

- All metal parts of mountings and structures should be protected by hot-dip galvanizing with zinc thickness of 60μm. The mountings must be protected against corrosion by protective artificial resin paint or non-staining colorless coating, in a dark-gray tone.

- From the top side, the post must be protected from rain, i.e., closed with a plastic plug or welded.

- A single post tubular mounting must be provided against swaying in the wind by the bars in the foundation.

- The posts are placed in the concrete foundation of quality MB 20.

- Execute the excavation of the foundation pit, and then concrete the base of the post, loaded with concrete MB 20, together with the steel post.

1.8.2 Truss mountings

- The truss mountings are made of a steel-drawn tube of uniform cross-section and thickness, depending on the number, type, and area of the signs that are placed on the mounting, which is indicated in the specifications, or the bill of quantities of the mountings in the design.

- All metal parts of mountings and structures should be protected by hot-dip galvanizing with zinc thickness of 60μm. The mountings must be protected against corrosion by synthetic resin protective paint or colorless plastification, in a dark-gray tone.

- From the top side, the post must be protected against rain, i.e., closed with a plastic plug or welded.

- Truss mountings are designed and executed separately, according to the signs they wore and based on the measures given in the traffic design.

- All the above elements are made following the specification, based on the static calculation that is an integral part of the design.

- The posts are placed in the concrete foundation of quality MB 20.

- Execute the excavation of the foundation pit, and then concrete the base of the post, loaded with concrete MB 20, together with the steel post.

QUALITY CONTROL

The manufacturer must possess an attestation for all materials used in the construction of traffic signs mountings.

CALCULATION OF WORKS

The price of single-post and truss mountings includes the following works:

- procurement of a traffic sign mounting, as well as quality control

1.9 Foundation works and installation of traffic signs

1.9.1 Foundation works of traffic signs

The foundation works consists of two phases:

- Earth works - include the excavation of earth or other material, for foundations, transport to dump or spreading of materials on the surrounding terrain. Works are calculated per m3 of excavated material.

- Concrete works - procurement, transportation and installation of concrete mark minimum MB 20 for tubular mountings and MB 25 for truss mountings.

1.9.2 Installation of the mountings

The placing of traffic signs mountings or anchor chairs in the concrete foot and assembly of the post on the foundation (includes the transport of posts and workers from the point to the place of work, placing the post or anchor chair in the molten foundation, fixing the post until the concrete is hardened. After hardening of the concrete, mount the post with anchor plate on the foundation).

The calculation for each type of work is done by the piece (s) of the traffic sign mounting and the concrete foot for the traffic signs.

1.10 Signs with changeable message content

DESCRIPTION

Traffic signs activated by a vehicle

Interchangeable traffic signs must be made following SRPS EN12966, which is proved by a certificate issued by an authorized body.

The interchangeable traffic signs that are activated by the coming of vehicles are used to draw drivers attention to adjust speeds on dangerous road sections.

Due to low power consumption, the vehicle-activated signs can be solar powered.

BASIC CHARACTERISTICS

A changeable traffic sign with a built-in Doppler radar. It is intended for use in the streets of cities and open roads, according to SRPS EN 12966 standard.

The optical and mechanical characteristics of the sign are in accordance with SRPS EN 12966.

Modular design allows for easy maintenance and replacement of parts.

When detecting irregular speeds, the sign lights up and displays the predefined symbol.

FUNCTIONAL CHARACTERISTICS

The following devices have the following characteristics:

• Automatic illumination control according to the time of day based on the precise algorithm

• Control and monitoring of the temperature inside the device

• Continuous diode excitation which ensures greater durability of LEDs

• Diagnostic software for checking and listing errors

• Transition effects with programming intervals increase visibility

• Traffic data sorted by the hour for one year can be downloaded for further analysis

• A large number of memory data that can be used to solve problems, statistical analysis, and system upgrades

• Real-time clock with precision 2ppm

• Possible communication interfaces: Ethernet. TCP / IP communication protocol

• Weight: approx. 20kg

• Maximum sign consumption: 20W

• Power supply: solar 12VDC

A solar package consisting of:

A solar panel of 100W, and an aluminum box containing a 55Ah battery and a charge controller.

Characteristics of radar detector

Sensor type: Doppler radar

Detection distance: 200m

Mechanical characteristics

Size: 850x850mm

Housing material: Aluminum case AlMg3, protection of plastics

The sign is resistant to the constant presence of dust, rain and/or snow min P3 according to SRPS EN12966

Service opening - from the front of the sign

Physical performance: T2 (according to SRPS EN12966)

Optical characteristics

Optical performance according to SRPS EN12966: L3, R2, B4, C2

Great and uniform contrast at all lightings

Diodes protected with UV protection lenses

The current excitation of diodes so that the lighting does not depend on the voltage

Symbol View

The symbol shows one symbol.

Side of square / circle: 600 mm

A possible mode of operation

Traffic sign activated by the vehicle measures the speed of the approaching vehicle; if the measured speed is greater than the predefined, the sign is activated. The sign activation threshold can be set a little more or less than the allowed speed. Usually, the sign is adjusted so that it is activated when the speed is 1 km / h higher than permitted in the direction on which the sign is placed. If the sign is set in this way, only vehicles that are moving at unallowed speed will activate the sign.

The sign is placed on a semi-portal G mounting, where the height from the carriageway surface to the lower edge of the sign is min 5m, and the range of mounting is 4m.

When there is no vehicle or when the vehicles are moving at speed lower than the defined by sign (the speed that activates the sign), the sign is turned off. When the vehicle runs at a higher speed than the speed that activates the sign, the sign lights up and alternately displays the predefined symbol, the II-30 "speed limit" (80 km / h).

Semi-portal mountings

- Semi-portal mountings are made of several steel drawn single-cross-section boxes and thicknesses to which the tubular mountings without construction or tubular mountings with construction are installed, depending on the number of boards and the size of the boards that are placed on the mounting, as indicated in the specifications, i.e., bill of quantities for the mountings in the design.

- All metal parts of mountings and structures should be protected by hot-dip galvanizing with zinc thickness of 60μm. The mountings must be protected against corrosion by protective artificial resin paint or by colorless plastification, in a dark-gray tone.

- Semi-portal mountings are designed and executed separately, according to the sign they wear and based on the measures given in the traffic design.

- Semi-portal mountings are made with an appropriate baseplate placed on an anchor plate with anchors on the foundation.

- All the above elements are prepared under the specification, based on the structural calculation that is an integral part of the design.

- The anchor plate is placed in the concrete foundation of quality MC 25.

- Execute the excavation of the foundation pit, and then concrete the base of the post, with plain concrete 25 MC, together with the anchor plate.

The foundation works consists of two phases:

- Earth works - include the excavation of earth or other material, for foundations, transport to dump or spreading of materials on the surrounding terrain. Works are calculated per m3 of excavated material.

- Concrete works - procurement, transportation and installation of concrete mark minimum MC 25.

QUALITY CONTROL

Before installing a sign with changeable content, semi-portal mounting, and other equipment, the contractor shall demonstrate its quality with an attestation, which will be presented to the supervisory authority.

MEASUREMENT AND CALCULATION

The price of traffic signs with interchangeable message content includes the purchase of LED traffic signs with variable content, supply of solar power supply, purchase of semi-portal mountings and concrete foot, preparation of the ground, installation of concrete foot, installation of semi-portal mounting, assembly of LED traffic signs with changeable content, assembly of solar panel, connection of facilities and equipment and commissioning of the system, as well as the cost of controlling the quality of materials used.

The calculation is done by piece (s) of an embedded traffic sign with interchangeable content with radar and a set of built-in solar panels.

- ROAD MARKINGS

Road markings are marked on roads with modern pavements. The application of the materials for their performance are set out in Table 1.

Road markings applied:

- Longitudinal markings SRPS U.S4.222, SRPS U.S4.223, and SRPS U.S4.224

- Cross markings SRPS U.S4.225, SRPS U.S4.227, and SRPS U.S4.228

- Other markings SRPS U.S4.229 to SRPS U.S4.233

- The procedure and equipment for application of coating for the markings on the road must be such that the works do not affect the safe traffic and safety of the contractor.

- The equipment must allow application of reflective spheres by injection (spraying), which significantly contributes to the durability of night visibility of signs. If the color is used with pre-mixed glass beads, surface spreading of beads on the applicated layer must also be carried out.

- The widths, colors, and timing of breaks are given on the situation in the graphic part of the design.

- The material, performance technology, and other color properties are prescribed by SRPS Z.S2.240.

- Road markings are plotted as thick-layered - the thickness of the sign dry layer (coating) should be higher than 0,80 mm thick.

- Road markings are done in white and yellow colors, but the markings must not increase the slipperiness of the carriageway.

- The marks should be performed with stable oil paint for this type of work, and painting should be careful without breaks and smearing.

- The composition of the material and the manner of making the markings must be such as to provide the reflective properties of the markings, as defined in Table 1.

- Road markings must retain at least 85% of their area at the end of the warranty period, and at the end of that period, these must not have less retroreflective values ​​than those provided for in Table 1 (in accordance with the Rulebook).

- The edges of the lines and figures must be sharp and even, with a deviation from the designed line, not more than 5 mm. The allowed differences from the given measures given in the design amount to a maximum of 5%.

- After applying of the markings on the road, the time until the moment when the traffic can take place over the marking, or the duration of the traffic restriction over the carriageway, may be up to 45 minutes.

- The yellow color is used to mark the bus stop. The paint for the performance of the elements mentioned above should be made on the basis of natural and artificial resins with additives. The paint must have reflex characteristics attained by adding reflective grains (beads) of at least 100 grams per kilogram of paint.

- Cold plastic (agglomerate) is used in the school zone for marking "X," the inscription "SCHOOL" and the sound-vibrating strips, as well as for marking the signs on the carriageway in the node 1307 (crossroads of state roads IB 13 and IB 15) as indicated in the situational plan.

- The work is carried out by machine and manually.

Table 1. Characteristics of material for permanent road markings

| Communication type |  | RL White | RL Yellow | RW (if Applied Type 2 markings) | Qd White | S*** (SRT units) |
| --- | --- | --- | --- | --- | --- | --- |
| Highway | *New markings | ≥300 | - | ≥100 | ≥160 | ≥50 |
|  | The minimum allowed value during use | ≥150 | - | ≥50 | ≥130 | ≥45 |
| Other state roads of the I class | *New markings | ≥300 | ≥200 | ≥75 | ≥160 | ≥50 |
|  | The minimum allowed value during use | ≥150 | ≥100 | ≥35 | ≥130 | ≥45 |
| State road of the II class | *New markings | ≥200 | ≥150 | ≥50 | ≥130 | ≥50 |
|  | The minimum allowed value during use | ≥100 | ≥80 | ≥35 | ≥100 | ≥45 |
| Claimed roads | *New markings | ≥200 | ≥150 | ≥50 | ≥130 | ≥50 |
|  | The minimum allowed value during use | ≥100 | ≥80 | ≥35 | ≥100 | ≥45 |
| Primary communications in settlement | *New markings | ≥200 | ≥150 | ≥75 | ≥130 | ≥50 |
|  |  | ≥100 | ≥80 | ≥35 | ≥100 | ≥45 |
| Secondary communications in settlement | *New markings | ≥150 | ≥100 | - | ≥130 | ≥50 |
|  | The minimum allowed value during use вредност године | - | - | - | ≥100 | ≥45 |
| RL – retroreflection coefficient (mcd x m-2 x lux-1); RW – retroreflection coefficient at wet conditions (mcd x m-2 x lux-1); Qd – illumination coefficient at difuse lighting (mcd x m-2 x lux-1); S – slipping resistance value (SRT) |  |  |  |  |  |  |

- The works are carried out in a dry period at an air temperature of +10 ºC to +30 ºC, relative humidity of 85% maximum and a carriageway temperature of +5 ºC to +45 ºC

- Before applying the paint, the surface of the pavement must be completely dry, clean, free from dust and the rest of the salt. Oil and other grease spots must be removed.

QUALITY CONTROL

The quality control of the materials used for the performed painting works is carried out according to SRPS U.S2.240. For all painting works, the warranty period must be at least 12 months.

The quality of the derived markings in the field must be verified and confirmed in one of the recognized laboratories.

Other materials must meet the requirements for certain durability and quality, and for each element, the contractor must provide an attestation.

The quality control of used road paints and executed works are carried out according to SRPS U.S2.240. For all works, the warranty must be at least 12 months.

CALCULATION OF WORKS

The prices of works for the road marking are calculated per square meter (m2) of the marked area. The specification also shows the total length of longitudinal markings on the carriageway. The price includes field grading, roadway cleaning, and degreasing, marking and quality control of used materials and works according to SRPS EN 1436 standard and SRPS U.S2.240.

6. TRAFFIC SIGNALS ON THE ROAD

This position includes the production, procurement, and installation of the following traffic equipment:

6.1. Traffic signals on the road for marking the edge of the carriageway

6.1. Traffic signals on the road for marking the edge of the pavement

Guard posts

DESCRIPTION OF POSITION

The position includes the preparation, procurement, and installation of guard posts. The number of guard posts is displayed in the Bill of quantities.

MATERIALS

The guard posts must be visible in all weather conditions, especially in case of reduced visibility (night, fog, snow, etc.) with their shape, measures, and method of production. The guard posts are set up so that participants in traffic in night hours and conditions of insufficient visibility will be able to spot the contours of the road on time.

PRODUCTION AND ASSEMBLY

Guard posts are set, according to the situational plan in the project. Guard posts are arranged according to valid standards with reflective fields of class 2 material. Guard posts must have reflective bodies of a specific surface (foils or other reflecting bodies), as follows: red on the right-hand side and white on the left-hand side in the course of vehicle movement. Guard posts are made according to standard SRPS.Z.S2.235.

QUALITY CONTROL

Before installation of the guard post, the contractor will prove their quality with an attestation, which will be presented to the supervisory authority.

CALCULATION OF WORKS

The price of the guard post includes the following works:

Procurement of guard post per piece (pcs);

placement of the guard post per piece (pcs). (The price of the guard post includes: transportation of guard post and workers from the point to the place of work, manual installation, guard post placing).

Catadiopters

On sections where there is a protective fence for vehicles, only night marks of reflecting bodies - catadiopters are placed on special mountings of metal or plastic - prisms, which are installed in the fence groove so that they cover the prescribed angle.

In the fence groove are installed catadiopters, the color of which is as the color of guard post (red and white).

If the fence is in the direction, the catadiopters are:

- on protective safety fences with protection levels H1 and N2 at a distance of 12 m;

QUALITY CONTROL

Before installing the catadiopter, the contractor will prove their quality with an attestation, which will be presented to the supervisory authority.

CALCULATION OF WORKS

The price of a catadiopter includes the following works:

- procurement of catadiopter per piece (pcs);

- the placing of catadiopter per piece (pcs). (The cost of a catadiopter includes: the transport of catadiopter and workers from the point to the place of work, manual installation, installation of the catadiopter).

7. ROAD EQUIPMENT

7.2 Safety fences (guard-rails)

DESCRIPTION OF THE POSITION

The position includes the production, procurement, and installation of a protective steel fence for vehicles, in all according to Serbian standards. The type of the fence is defined in the bill of quantities of this design and according to the classification given in the Technical Instructions for the Implementation of the Vehicle Retention System on the state roads of the Republic of Serbia issued by JP Putevi Srbije and the standard SRPS EN 1317.

MATERIALS

The material for production each of the elements of the protective fence in all must comply with the requirements of standard SRPS EN 1317.

PRODUCTION AND ASSEMBLY

The fence is set according to the situation in the design. The location plan explicitly determines the length of the fence, the micro-location on which it is placed, the length of the fence ends, and the like.

The protective bumper of the fence is placed on posts of appropriate length so that the upper edge of the bumper is at the height of 0.75 m from the nearest edge of the pavement.

The fence must be protected from corrosion by galvanizing, at the choice of the investor. The terminal elements of the fence by the shape and length must meet the technical conditions for installation given in SRPS EN 1317. The length of the terminal elements is defined on the situational plan.

At the distance of 12 meters, the reflecting bodies-catadiopters are built into the groove of the fence, whose color is same as the guard posts.

The distance between the posts is 2.0 and 1.33 m.

The ends of the fence are carried by lowering and partial digging into the ground, and their length is defined in the situational plan.

QUALITY CONTROL

Before the installation of a protective fence, the Contractor shall prove its quality with an attestation, which will be presented to the Supervisory Authority.

CALCULATION OF WORKS

The price of the fence is calculated by the linear meter of the raised fence. The cost of terminal and transitional structures is calculated per piece.

7.5 Pedestrian fences

DESCRIPTION OF THE POSITION

The position includes construction, procurement, and installation: pedestrian fences with foundations.

MATERIALS

The metal pedestrian fence is made of steel following the requirements of the standard.

Foundations are made of concrete of the minimum mark MB 20.

PRODUCTION AND ASSEMBLY

The metal pedestrian fence should be installed as standard traffic posts and must be protected against corrosion by hot-dip galvanization following EN ISO 1461 standard.

The metal pedestrian fence should be set according to the situation plan.

QUALITY CONTROL

The manufacturer must possess an attestation for all materials used during the construction of the said traffic equipment.

CALCULATION OF WORKS

The price of a metal pedestrian fence includes the price of delivery and transport to the place of installation, installation, preparation of the ground, installation and leveling, as well as quality control of the materials used.

8. TECHNICAL MEANS FOR TRAFFIC DECELERATION

8.1 Vibrating strips

Vibrating strips are technical means for traffic deceleration, which, when are crossing by the vehicle, produce stronger vibrations and sound effects to warn drivers to reduce the speed of movement, or to harmonize driving with the prescribed speed limit.

The position includes the production, procurement, and installation of technical means for the traffic deceleration, hereinafter referred to as the vibrating strips, in a grid (3x2 strips), 3 m in length, width d = 12 cm. Vibrating strips are placed in pairs at a distance of 1.8 m (2.0 m), if necessary, can be repeated several times.

Vibrating strips are made of cold plastic. Cold plastic must be resistant to all atmospheric effects, UV rays, petroleum products, oils, salts and abrasion (wear).

Vibrating strips must have the necessary attestations from the competent authorities and laboratories to demonstrate their technical characteristics and guarantee the possibility of their use in the function of making technical means for the traffic deceleration.

The price is calculated by the linear meter of the placed strip. The price is expressed per linear meter, as well as the price of assembly, which includes all the necessary work, as well as all the costs required for the turnkey installation, which means that after the completion of the works by the contractor, the traffic can be normal and safe at places where vibrating strip is placed.

9. OTHER ROAD EQUIPMENT AND SIGN WORK

9.1 Traffic counter

DESCRIPTION

This position includes the procurement, delivery, and installation of inductive loops of traffic counters. The inductive loop wire must be made of copper, silver plated or nickel plated, with Teflon insulation, diameter 1.3 mm2. The wire must have the same or better quality than the wire bearing the mark LI5Y AVG 16/19E. The price includes purchase and delivery to the place of installation.

PRODUCTION

The installation of inductive loops is done exclusively by the technology of cutting the carriageway without knife wetting, or the "dry cutting" technology. The size of the inductive loops depends on the counting device operation method and vehicle classification and must be entirely in compliance with its characteristics. For the needs of installation, asphalt cutting is done at an optimum depth of not less than 4.5 cm. In cut grooves of 6 mm width, after cleaning and blowing, the wire is laid. After laying, the ends of the wire are twisted. At least 20 cm from the edge of the carriageway, a hole drilling is carried out through a pavement structure at an angle of 45 degrees. Through the holes, the euroflex tube of 12 mm in diameter is pulled through, and the inductive loop connectors within it. At a section between the foundation and the carriageway edges (to the loop connection), an excavation of a 60 cm deep trench is made. A tube of diameter 3.5 cm is laid in the ditch. It is made of alkaten, euroflex or okiten and through the inductive loops connectors are dragged, which later through the foundation and pillar lead to the devices in the assembly cabinet. The next step in the preparation is the sealing of the cut grooves with the appropriate mixture. The sealing mixture is a modified bitumen or a suitable two-component mixture. This position includes the transportation of the elements on the site and all work on the installation of inductive loops, that is, cutting the carriageway, pavement drilling, excavation of the trench, laying of tubes and pulling the connections through the foundation, as well as sealing of the cut grooves with the appropriate mixture. In addition to the above, the price includes the price of the sealing mixture as well as the tube min. diameter of 3.5 mm and all work on the pavement cleaning, landscaping of the location and planning of the dividing band.

QUALITY CONTROL

Before installing the inductive loop, the contractor shall prove its quality with an attestation, which he will present to the supervisory authority.

MEASUREMENT AND CALCULATION

The price includes all work on the installation of inductive loops and commissioning of the traffic counter.

9.2 Pedal cyclists counters

DESCRIPTION OF POSITION

The position includes the delivery and installation of devices for pedal cyclists counting with displays for the review of counted pedal cyclists, with all the necessary accompanying equipment and installation.

CHARACTERISTICS OF THE DEVICE, INDIVIDUAL ELEMENTS OF THE SYSTEM AND SYSTEM IN THE WHOLE

The necessary elements for the reliable operation of automatic counting of pedal cyclists are automatic counters of traffic (hereinafter referred to as counters) at the counting sites that make up the whole with displays for displaying the number of cyclists and accompanying counters in the form of power units, batteries, inductive loops, prefabricated cabinets, solar panels.

The counter must have an embedded GSM / GPRS module for communication with the central computer. Communication is done remotely via GPRS and includes automatic data transmission. Besides, the device must be able to remotely configure and calibrate, monitor operation and remote software changes. The device collects and records data on a memory card. The data for each vehicle is recorded separately as well as interval data in a pre-defined 15-minute record. When recording data on each vehicle, data on the day, time, minute and seconds of vehicle detection, as well as data on its speed of movement are recorded separately. When registering a vehicle in an interval record, the data on: the number of vehicles in the direction of flow, the speed distribution of speed classes, the minimum speed, the maximum speed, the average speeds, the time interval of the offset and the current condition of the device are recorded. In case of alarm, pre-defined condition of the device (inductive loop interruption, low voltage, wrong direction of movement of vehicles, etc.), the device must be able to send an SMS to predefined phone numbers. Interval data are collected automatically via GPRS communication via the central terminal. The memory capacity must be such that it can record all data for at least 30000 vehicles/day for all 365 or 366 days for each course of the vehicle movement in particular. The device must have the function of generating information about the current state of traffic and sending such information in the form used in the central terminal for reporting the current state of traffic. This information is sent every 5 minutes. The device for counting and classification of vehicles can be made in the form of one unit. The device must have at least 4 detection channels for connecting 4 inductive loops. Also, the device must have the ability for power supply by solar energy and the ability to power supply from the network without any changes in it (hardware or software).

PRODUCTION AND INSTALLATION

The counter with displays is placed on the foundation, and the casing must be prepared to accept the elements that are placed inside it and must be constructed, installed and additionally secured in accordance with the protection against vandalism. Inside the enclosure, a counter, a battery, a power supply unit (for power supply from the grid) and elements for interconnecting the system elements, as well as elements for protecting and fixing the elements of the system for the enclosure are placed.

The installation of inductive loops is done exclusively by the technology of cutting the carriageway without knife wetting, or the "dry cutting" technology. For the needs of making, asphalt cutting is done at an optimal depth of 3 to 5 cm. In cut grooves of 6 mm wide, after cleaning and blowing, the wire is laid. After laying, the ends of the wire are twisted and led to the housing. The next step in the preparation is the sealing of the cut grooves with the appropriate mixture. The sealing mixture is a modified bitumen or a suitable two-component mixture.

QUALITY CONTROL

The counter must have the appropriate CE certificate.

CALCULATION OF WORKS

This position includes the procurement, delivery, installation, assembly, calibration, configuration and commissioning of the counter, installation of cabinets and installation of inductive loops. The works on the installation of inductive loops represent a cutting of pavement, pavement drilling, excavation of the trench, and sealing of the cut grooves with the appropriate mixture. In addition to sealing, all works on cleaning of the carriageway, landscaping of the site and planning of the earth's surfaces, where changes occurred during the execution of the works, are counted.

9.3 Radar casing

DESCRIPTION

This position includes the purchase, delivery, and installation of the housing. The casing is used to fit the speed control device (radar) and the associated battery. The casing is made of metal or plastic materials with a degree of protection IP 55. On the opposite side of the door, there is a glass hole through which the device can record the speed of vehicles movement without interferences.

The casing must be pre-prepared for mounting on the post, accepting the elements that are placed inside it and must be constructed, installed and additionally secured in accordance with the protection against vandalism. All elements used to make the interior of the casing, for mounting on the post and for the prevention of vandalism, must be made of anti-corrosive materials (stainless steel or aluminum) that are additionally protected by high-quality paint in the powder-based plastification process.

INSTALLATION

The casing is placed on a semi-portal post of changeable removable traffic sign works next to the carriageway. The housing should be so positioned that the glass opening is oriented in the direction towards the orientation of the changeable traffic sign.

QUALITY CONTROL

Before installing the casing, the contractor will prove his quality with an attestation, which he will present to the supervisory authority.

MEASUREMENT AND QUALITY

The price of the casing includes the purchase and delivery to the place of installation, all fastening elements for the carrier, assembly of the housing on the built-in G mounting of changeable traffic sign works, as well as quality control.

10. OTHER WORKS

10.1. Dismantling and removal of traffic signs and billboards

DESCRIPTION

The contractor is obligated to safely remove all elements of the sign, accessories, and sign, to remove the post with concrete foundation and to fill the hole of the foundation and to restore the shoulder into the proper condition. All elements of the damaged post and the old foundation should be removed in a place designated by the supervisory authority. All dismantled elements are transported to the Contracting authority’s warehouse according to the order of the Supervising Authority, while the surplus of material resulting from the demolition or removal is transported to a dump designated by the Supervisory Authority.

MEASUREMENT AND CALCULATION

The price of the works includes all necessary work for its execution in full with all the costs of loading and unloading, dismantling and transport, as well as repairs of the shoulder, while the calculation is shown by piece.

10.2. Removal of the road markings

Existing traffic signs on the carriageway, which do not fit into the design solution, should be deleted by scraping from the carriageway or by painting with stable paints in the existing pavement colors. Works on the removal of existing horizontal signaling on a carriageway are calculated per m2 of scrapped or painted surface of a carriageway.

10.3. Dismantling and removal of safety fences

DESCRIPTION

The Contractor is obligated to safely remove all existing elements of the safety fences, accessories, and posts. The dismantled fence and other damaged elements of the same, with elements of post foundations, should be removed in a place designated by the supervisory authority.

MEASUREMENT AND CALCULATION

The price of works on the dismantling of the safety fence is done per linear meter with all the costs of loading and unloading, dismantling and transport, as well as repairs of the shoulder.

1. TRAFFIC SIGNS

DESCRIPTION OF POSITION

The position includes the production, purchase, and installation of standard traffic signs (signs that are made in detail according to detailed drawings in Serbian standards, under names, code, and appearance following the Traffic Signaling Rulebook).

Traffic signs include:

- Warning signs

- Regulatory signs

- Information signs

- Supplementary boards

MATERIALS

Standard signs are made from materials and in the manner prescribed in SRP EN 12899 (Technical requirements - general requirements for preparation and testing). Standard traffic signs are made from an aluminum sheet, or galvanized steel sheet, according to the choice of Investor.

PRODUCTION AND ASSEMBLY

The size of the standard traffic signs is in the function of their shape and the rank of the road on which these are located.

Traffic signs have dimensions that meet the traffic conditions on the designed section.

Standard signs are all made according to the details of the drawings in Serbian standards, under the names, code, and appearance according to the Traffic Signs Rulebook (SRP Z.S2 from 301 to 309).

There must be no fixation on the face of the sign (screws, bolts, etc.), which would interfere with the legibility and reflection of the sign, both in daylight and in the lighting of the car's headlights.

The back of the sign, including all the fastening elements on the mounting, must be protected with synthetic resin paints in a dark-gray tone.

The signs are attached to a single-tube mounting using clips placed on the back of the sign.

The signs must be secured against swaying and shearing by inserting a plastic cuff between the clip and the post - (unless the sign mounting is coated).

If new traffic signs are being set, the manufacturer is obliged to print on the back of the sign the sign code according to the Traffic Signaling Rulebook, with the possible content (numerical or inscription) in the building; if a sign is placed in an opaque wrapper, the obligation applies to the wrapper also.

If new traffic signs are being set, the manufacturer is obliged to deliver the signs in the protective wrapper, on which the sign code number must be printed.

QUALITY CONTROL

The manufacturer must possess an attestation for all materials used in the production of standard traffic signs. Quality control is performed in accordance with SRPS EN 12899.

CALCULATION OF WORKS

The price of the standard traffic sign includes the production and delivery of the sign, all elements for fastening on the mounting (reinforcement, clips, screws, cuffs, etc.), as well as quality control according to SRPS EN 12899.

1.8 MOUNTINGS OF TRAFFIC SIGNS

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of traffic signs mountings:

1.8.1. Single-post tubular mountings

Post tubular mountings are made of a steel-drawn tube of uniform cross-section and thickness, depending on the number and type of signs that are placed on the mounting, which is indicated in the specifications, or the bill of quantities of the mounting in the design.

All metal parts of mounting and structures should be protected by hot-dip galvanization with zinc thickness of 60 μm. The mountings must be protected against corrosion by protective artificial resin paint or by paint-less plastification, in a dark-gray tone.

From the top the post must be protected from the rain, i.e., closed with a plastic plug or welded.

A single-post tubular mounting must be secured against rotation.

Posts are placed on mobile platforms.

1.8.2 Truss mountings

The truss mountings are made of a steel-drawn tube of uniform cross-section and thickness, depending on the number, type and surface area of the signs that are placed on the mounting, which is indicated in the specifications, i.e., in a bill of quantities of the mountings in the design.

All metal parts of mountings and structures should be protected by hot-dip galvanization with zinc thickness of 60μm. The mountings must be protected against corrosion by protective artificial resin paint or paintless plastification, in a dark-gray tone.

From the top the post must be protected against the rain, i.e., closed with a plastic plug or welded.

Truss mountings are designed and executed separately, according to the sign they bore and based on the measures given in the traffic design.

All the above elements are made following the specification and based on the structural design that is an integral part of the design.

The posts are placed in the concrete foundations of quality MB 25.

Perform the excavation of the foundation pit, and then concrete the foundation of the post, with bulk concrete 25 MB, together with the steel post.

QUALITY CONTROL

The manufacturer must possess an attestation for all materials used in the construction of traffic signs.

CALCULATION OF WORKS

The price of single-post and truss mountings and portable stands includes delivery and transport to the place of installation, the price of accessories for connections between the mounting elements, the staves in the mobile stand, as well as the price of the mounting seal gaskets as well as the quality control of the materials used.

1.9 FOUNDATION WORKS AND INSTALLATION OF TRAFFIC SIGNS MOUNTING

1.9.1 The foundation works of traffic signs

The foundation works consist of two phases:

- Earth works - include the excavation of earth or other material, for foundations, transport to the dump or spreading of materials on the surrounding ground. Works are calculated per m3 of excavated material.

- Concrete works - procurement, transportation and installation of minimum mark MB 25 for truss mountings.

1.9.2 Placing of the mounting

Installation of the anchor chairs in the concrete foot and assembly of the post on the foundation (it includes the transport of the post and workers from the point to the place of work, the anchoring of the chair in the cast foundation, the fixing of the post until the concrete is hardened. After hardening of the concrete, installation of the post with anchor plate on the foundation).

The calculation for each type of work is done by the piece (s) of the traffic sign mounting and the concrete foot for the traffic signs.

1.9.3. Mobile stands for traffic sign mountings.

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of mobile stands and sandbags.

PRODUCTION

The mobile stands are made of concrete, solid metal, plastic or other modern materials that ensure the stability of the set sign works. On mobile stands with 2.5 m mountings and longer, two sandbags are placed to provide their additional stability. The bags are from nylon, filled with 50 kg of sand.

QUALITY CONTROL

The manufacturer must possess an attestation for all materials used in the manufacture of mobile stands.

MEASUREMENT AND CALCULATION

The price of portable stands and sandbags is calculated according to the piece of set elements.

2. THE ROAD MARKINGS

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of materials used for the construction of elements of horizontal traffic sign works, i.e., marking of the carriageway.

MATERIALS

The material used to produce horizontal traffic sign works elements may be of the following types of material:

- Applicative materials (strip) which are installed by cementation on a carriageway,

- Road paint

The applicative material (strip) must be extremely durable. It must be retroreflective, appropriate resistant to slip and it must be yellow. Applicative materials must possess retroreflective properties, according to SRPS EN 1436. Also, these must have the possibility of removing (de-cementation) without damaging the carriageway.

The material, performance technology and other properties of the road paint are prescribed by SRPS U.S2. 240.

PRODUCTION

The works are carried out according to detailed drawings, and location plans from the traffic sign work design.

Applicative strips can be placed (cemented) during the construction of an upper, hot asphalt layer or can be installed over already made asphalt.

The materials must have the prescribed slip resistance coefficient class S1, SRT ≥ 45, whereas night retroreflection must be of class R5 ≥300 mcd • m-2 • lx-1.

The thickness of elements painted with road paint must be at least 600 microns, which corresponds to a paint consumption of 1 kg/m2 and reflective beads of 400 g/m2 of painted surface.

All painted surfaces must have a prescribed adhesion friction coefficient, which must not be less than the adhesion friction coefficient of the pavement.

The edges of the lines and figures must be sharp and straight, with a deviation of the designed line of not more than 5 mm. Permitted deviations from the measures given in the design amount to a maximum of 5%. The work is carried out by machine or manually.

QUALITY CONTROL

All materials must satisfy the requirements for certain durability and quality, and for each article, the contractor must provide an attestation.

CALCULATION OF WORKS

The prices of works on the implementation of horizontal signal works are calculated per m2 (square meter). The price includes terrain grading, cleaning, and degreasing of pavement, application of adhesive strips, painting and quality control of used materials and all types of works on the installation of materials.

- TRAFFIC LIGHTS

3.1 TRAFFIC LIGHTS FOR VEHICLE MOVEMENT CONTROL

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of a traffic light: a traffic light for vehicle movement control (mobile traffic light with power supply).

MATERIALS

Illuminated signs must be made of such material and in such a way as to ensure reliable operation even in the most unfavorable weather and climatic conditions

PRODUCTION AND ASSEMBLY

Vehicle movement control traffic lights are provided with three-colored LED lights (mobile traffic lights) with a lantern diameter of at least 300 mm for a red light and 210 mm for the yellow and green light. The traffic lights are positioned on the right-hand side of the traffic lane used for traffic from the direction of travel to which the signal relates. Traffic lights must be connected by cable or radio connection to a common control device. The control of the operation of traffic lights for alternating yieldance of vehicles is carried out automatically, according to the program built into the controller.

QUALITY CONTROL

Before the installation of light signals, the contractor will prove their quality with an attestation, which will be presented to the supervisory authority.

CALCULATION OF WORKS

The price of illuminated signs includes the cost of their purchase, shipping and delivery costs to the place of installation, installation, and programming of the traffic light device.

5. TEMPORARY TRAFFIC SIGN WORKS

5.1. FRONTAL BARRICADES

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of barricades.

MATERIALS

Frontal barricades are made of plastic materials, aluminum or galvanized steel sheet. The mobile stand is made of solid plastic materials, rubber, concrete or metal.

PRODUCTION AND ASSEMBLY

Frontal barriers are placed according to situations and detailed drawings in the design.

Frontal barriers are placed normal to the road axis that is closed for traffic as well as along the edge of the construction site.

Frontal barriers are covered with a reflective Class II film. These are installed at the height of 1.0 m from the surface of the carriageway, on mountings made of metal pipes. The mountings are embedded in portable stands made of solid plastic, concrete, metal or rubber.

Frontal barriers are placed according to the location plan.

QUALITY CONTROL

Before the installation of frontal barriers, the contractor will prove their quality with an attestation, which will be presented to the supervisory authority.

CALCULATION OF WORKS

The cost of horizontal barriers is calculated per piece.

5.2. HORIZONTAL BARRIERS

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of horizontal obstacles.

MATERIALS

Horizontal barriers are made of plastic materials, aluminum or galvanized steel sheet. The mobile stand is made of solid plastic materials, rubber, concrete or metal.

PRODUCTION AND ASSEMBLY

Horizontal barriers are placed according to situations and detailed drawings in the design.

Horizontal barriers are placed perpendicular to the axis of road closed for traffic, as well as at the edge of the construction site when it is necessary to ensure the safety of pedestrian traffic that is taking place next to the site.

Horizontal barriers are coated with reflective Class II film. These are installed at the height of 1.0 m from the surface of the carriageway, on mountings made of metal pipes with a diameter of 50 mm. The mountings are mounted in a movable stand made of solid plastic, concrete, metal or rubber.

Horizontal barriers are set in everything according to the location plan.

QUALITY CONTROL

Before setting horizontal barriers, the contractor will prove their quality with an attestation, which will be presented to the supervisory authority.

CALCULATION OF WORKS

The cost of horizontal barriers is calculated per piece.

5.3. VERTICAL BARRIERS

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of vertical barriers.

MATERIALS

Vertical barriers are made of plastic materials, aluminum or galvanized steel sheet. The mobile stand is made of solid plastic materials, rubber, concrete or metal.

PRODUCTION AND ASSEMBLY

Vertical barriers are set according to situations and detailed drawings in the design.

Vertical barriers are coated with Class II reflecting foil. These are set to mark the edges of the site and to guide the traffic. The vertical barriers size is 0.25 x 1.00 m and the total height is 1.30 m.

Vertical barriers are placed at the mutual distance in everything according to the location plan.

QUALITY CONTROL

Before installing vertical barriers, the contractor will prove their quality with an attestation, which will be presented to the supervisory authority.

CALCULATION OF WORKS

The price of the vertical barriers is calculated by piece.

5.4. OBSTACLE STRIPS

DESCRIPTION OF POSITION

The position includes the production, procurement, and assembly of the obstacle strips.

MATERIALS

The obstacle strip is a strip of plastic film with alternating fields of red and white color.

PRODUCTION AND ASSEMBLY

The obstacle strips are placed according to the situation in the design.

These are set to indicate the edge of the site, i.e., the separation of the construction site from the pathway.

QUALITY CONTROL

Before setting up the obstacle strips, the contractor will prove its quality with an attestation, which will be presented to the supervisory authority.

CALCULATION OF WORKS

The price is calculated by the meter of the used obstacle strips

5.9 FLASHING LIGHTS

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of light signs for marking works on the road.

MATERIALS

Illuminated signs must be made of such material and in such a way as to ensure reliable operation even in the most unfavorable weather and climatic conditions.

PRODUCTION AND ASSEMBLY

In places where it is not possible to secure a grid power supply, suitable battery batteries can be used to the power supply of the illuminated signs.

Flashing lights are placed on barriers, obstacles or special mountings.

QUALITY CONTROL

Before the installation of illuminated signals, the contractor will prove its quality with an attestation, which will be presented to the supervisory authority.

CALCULATION OF WORKS

The price of illuminated signs includes the costs of their purchase, shipping and delivery costs to the place of installation and its installation.

5.12 FLAGS FOR HAND-SIGNALING CONTROL OF TRAFFIC

DESCRIPTION OF POSITION

The manual control of traffic in the work zone is done by at least two designated workers of the contractor, in a manner to face the traffic and extend the flag toward vehicles. Traffic control is done with flags of red and green color of at least 40cm x 40cm.

Traffic control is performed with flags of red and green color of dimensions of at least 40 cm x 40 cm, which have the following meaning:

1) raised green flag - free passage for vehicles from the direction where this flag was raised,

2) raised red flag - prohibited passage for vehicles from the direction where this flag was raised.

In the case where the flaggers do not see each other, a radio link is used for their communication.

CALCULATION OF WORKS

The price of the traffic control by the flags is calculated by the number of the flag and the number of engaged people per day (people/days).

8. OTHER WORKS

8.1 OVERLAY OF TRAFFIC SIGNS

DESCRIPTION OF POSITION

Temporary overlay of traffic signs is done to suspend the validity of existing permanent traffic signs. To achieve this, it is necessary to overlay the sign symbol with a suitable non-transparent foil or a sign overlaying strap.

PRODUCTION AND ASSEMBLY

The contractor is obliged to perform a safe and adequate installation of an opaque film or a covering strap to suspend the traffic sign in both day and night conditions. After completion of the works, the traffic sign must be restored to its original state (unless otherwise specified by the design).

CALCULATION OF WORKS

The price of the traffic signs overlaying is calculated according to a piece of covered traffic signs.

8.2 REMOVAL OF TRAFFIC SIGNS

DESCRIPTION OF POSITION

The contractor is obligated to safely remove all elements of the sign, accessories, and sign, to remove the post with concrete foundation and to fill the foundation pit and to bring the shoulder to the correct state. All elements of the damaged post and the old foundation should be removed in a place designated by the supervisory authority. All dismantled elements are transported to the Contracting authority’s warehouse according to the order of the Supervising Authority, while the surplus of material that has been created by demolition or removal is transported to a dump designated by the Supervisory Authority.

CALCULATION OF WORKS

The price of the works includes all necessary work for its execution in full with all the costs of loading and unloading, dismantling and transport, as well as repairs of the shoulder, while the calculation is shown by piece. The calculation of the performed works is done according to the piece of the removed and deposited traffic sign, and according to the above description.

8.3 REMOVAL OF THE ROAD MARKINGS

DESCRIPTION OF POSITION

The contractor must carry out the removal of the markings on the carriageway using equipment designed specifically to remove markings, and not using a milling machine to increase roughness or remove asphalt. Road markings are removed in a way that does not damage the road.

CALCULATION OF WORKS

Calculation of performed works is done per square meter (m2) of removed markings on the road.

8.4 PLATFORM FOR VEHICLES

DESCRIPTION OF POSITION

The position includes the production, procurement, and installation of the platform (temporary assembly vehicle crossing).

MATERIALS

Platforms can be made of wood or metal.

PRODUCTION AND ASSEMBLY

Platforms can be made of wood or metal so these should have the proper carrying capacity and dimensions for the traffic flows of the vehicles that occur at the place where the platforms are placed. The size of the platforms for vehicles must not be less than 2,5 x 3,0 m.

The platforms are sized based on field needs and traffic loads. It is necessary to ensure that the platforms are stable, that they do not slip on the surface where they are positioning and that these themselves are not slippery for vehicles that cross over them.

CALCULATION OF WORKS

The price of the platform is calculated per piece.

8.5 EARTH WORKS

Excavation of humus

DESCRIPTION OF POSITION

The excavation of humus should be performed by a mechanical 95% and manually 5% and within the designed depths and widths below and above the road base. Only after the marking of the designed widths, an inclination of the slopes and the site surveying along the transversal profiles, the hummus can be removed. The thickness of the humus layer to be removed is determined as a rule by design on the basis of geomechanical testing, and it is also determined on the spot together with the supervisory body by profiles or sections of the road. If the need for changing the thickness is established during the construction, this supervisory body will enter this change in the construction book. Humus pushing must be carried out in such a way that it does not mix with the land for the embankment, as well as to allow drainage of the road base. The excavated humus in the amount to be used for topsoiling of green surfaces, shoulders, and slopes should be deposited in the correct figure, and the excess prepared for transport.

CALCULATION OF WORKS

Calculation of performed works is done per cubic meter of removed self-sprouted humus with pushing up to 10 m for all work and material.

8.6 PAVEMENT CONSTRUCTION

DESCRIPTION OF POSITION

The work includes the procurement and installation of granular rock material. Works can only begin when the supervisor accept a subgrade regarding evenness, designed levels, slopes, and compactness. Materials for the production of a bearing layer can be natural gravel, crushed rock material, a mixture of natural gravel and crushed material and mixtures made up of several fractions. All of the above materials must meet certain conditions regarding mechanical characteristics, granulometric composition, carrying capacity and other states according to the applicable standards.

On the planned and rolling subgrade, grained rock material is applied, it is spread by a grader or other suitable means, it is wetted and compacted to the required compaction by suitable static and vibratory equipment. The bearing layer is carried out in layers of thickness from 20 to 40 cm, which is determined by design. The material must also meet the requirements for resistance against frost. The upper surface of the supporting layer should be made according to the designed levels and slopes, while the evenness of the finished layer is controlled by a staff of length L = 4m, and the allowed deviation is (+, -) 1cm. The inspection tests regarding compactness should be carried out with a circular plate of diameter d = 30 cm, and the smallest modulus of compressibility depends on the type of rock material:

- for natural gravel						Me = 50 MN/m2

- for a mixture of natural gravel and crushed material   	Ме=60 MN/m2.

- for crushed rock material					Ме=70 MN/m2

CALCULATION OF WORKS

Calculation of performed works is done per cubic meter (m3) of the finished carrier layer from mechanically compacted grained material, for all work, material, procurement, and transport of rock material and control tests.