# VOLUME 3

# TECHNICAL SPECIFICATIONS

- 1. TECNICAL DESCRIPTION OF CONTRUCTION WORKS ON HEAVY MAINTENANCE OF ROAD

- 1.1. PREPARATORY WORKS

- THE ALIGNMENT AND FACILITIES MARKING AND SETTING OUT

Prior to work commencement, the Contractor is obliged to perform all the necessary road, intersection, and structure axis marking. It is done based on the marking plan from the design. During the execution of works, polygon points, benchmark, and fixed points should be secured. If the Design does not provide data on polygonal points and benchmarks, obtain them from the competent company for self-setting out.

Calculation of executed work is done per running meter of set out alignment.

- CUTTING TREES

Cut down trees in width of the zone covered by construction of the road body. Trees should be cut mechanically in height of up to 80 cm from the ground and carefully put trees down. Then cut branches, sort the timber and prepare for transport. Determine the place of depositing in agreement with the supervisory authority. During works, take precautionary measures in order to avoid possible damage to neighbouring buildings/facilities and property in general.

The calculation of work is done per piece of cut tree for all work, material and transport, and according to the abovementioned description and the diameter of trees.

- REMOVAL OF STUMPS AND ROOTS

Cut down trees in width of the zone covered by construction of the road body. Remove the stumps of cut trees and those that have been found there. Removal of stumps should be done by machine. The obtained timber shall be classified, loaded into means of transport, transported to a landfill that is determined by the supervisory authority.

The calculation of executed works is done per piece of removed stump for all work and material and transport, as described above.

- EXCAVATION FOR IDENTIFICATION OF UNDERGROUND INSTALLATIONS

This work includes manual excavations planned according to the Design or the request of the supervisory authority for the purposes of cutting grips and consequently, determining the position of installations. It is envisaged that 95% of excavation will be done manually and 5% by machine. Insert excavated earth material into figures suitable for loading.

- The calculation of executed works is carried out per cubic meter of excavated autochthonous material with a push of up to 20 m, prepared earth material for transport.

- DEMOLISHION OF PAVEMENT

The existing pavements of all kinds, which according to the Design should be removed, should be demolished mechanically together with the base of average thickness d=25-40 cm of different composition. Material obtained by demolition of the existing pavement should be loaded into a transport vehicle, transported to a landfill determined by the supervisory authority, unloaded and planned, or if it is possible, it can be used for embankment construction.

The calculation of executed works is carried out per cubic meter of demolished pavement for all work, material and transport, and according to the abovementioned description.

- CURB DEMOLITION

Existing curbs, irrespective of the type, which should be removed according to the Design, must be demolished manually along with the concrete base under the curbs. Clear demolished curbs from concrete and mortar, load into vehicle, transport to landfill, unload and arrange in proper figures. Detritus/debris made after demolition of curbs should also be loaded into the vehicle and transported to the landfill determined by the supervisory authority, unloaded and planned at the landfill.

If demolished curbs can be reused, they should be deposited at the site of new installation.

The calculation of executed works is carried out per running meter of removed curb, for all work, material and transport and according to the above said description.

- FOOTWAYS AND CYCLE LANES DEMOLITION

Demolish sidewalks and cycle lanes that are planned to be removed according to the Design. Average thickness of the base is 30-40 cm and has different composition. If the sidewalk is made with slabs, remove these slabs manually, clean and load them into the vehicle. Debris made after demolition should be loaded into the vehicle and taken to a landfill determined by the supervisory authority, unloaded and planned.

The calculation of executed works is done per square meter of demolished sidewalk or cycle lane for all work, material and transport, as described above.

PREPARATION OF CONSTRUCTION JOINTS TO CONTINUE ASPHALT WORKS

Regarding parts where the existing asphalt pavement is widened or extended according to the Design, asphalt pavement should be benched cut (d=6-10 cm) with a pneumatic hammer with a trowel or a circular cutter. The cutting line on the pavement surface should be straight. Cutting degrees in height are equal to the height of made layers, with a horizontal stretch of about 10 cm for asphalt layers. Material obtained after demolition must be loaded into a vehicle, transported to a landfill or used at a construction site.

The calculation of executed works is done by running meter of prepared pavement for continuation and according to the abovementioned description.

- SCRAPING OF ASPHALT LAYER

Scraping of asphalt in layers in a thickness of about 5 cm should be done on a part where pavement fits and where finish grade is raised in relation to the existing pavement or where there are ruts. Scraping or roughing of asphalt should be carried out in order to obtain a better connection between the existing pavement and the new layer of asphalt on the part where finish grade is raised. Scraped material should be transported to a place specified by the Design or at the request of the supervisory authority.

The calculation of executed works is done per square meter of scraped surface and the price includes the removal of scraped material.

- PROTECTION OF EXISTING UNDERGROUND INSTALLATIONS

Lay plastic or concrete cable ducts or semi cable ducts on planned and compacted surface of the trench, so that necessary installations can subsequently be placed in the trench, check the position and height of the elements and fill the trench with compaction.

The calculation of executed works is paid per running meter for all work and material, depending on the type of cable ducts or semi cable ducts.

- LEVELLING AND FITTING OF EXISTING MANHOLES

Existing sewage manholes, drains, pipeline manholes and TT columns/poles that do not correspond to the newly designed spot levels in their height position, fit with the appropriate lifting-lowering (10-20 cm) of the iron frame, with the demolition and construction of a concrete cushion below the frame. All material obtained after this job is loaded into a vehicle, transported to a landfill as directed by the supervisory authority, unloaded and planned.

The calculation of executed works is done per piece of regulated manhole and drain, for all work and material and according to the abovementioned description.

- DESIGN PREPARATION OF AS-BUILT CONDTION

After the completion of the road construction works, the Investor and the Contractor are obliged to prepare a design of the completed condition if there were significant changes in relation to the design solution.

The calculation of the performed works is done per route running meter for which the design of the as-built condition has been prepared.

ARCHAEOLOGICAL SUPERVISION FOR MONITORING OF EARTH WORKS

In accordance with a decision issued by the Intermunicipal Institute for the Protection of Cultural Monuments of Subotica, during earth works that include excavations larger than 15 cm below the surface layer, it is necessary to provide archaeological monitoring for monitoring earth works on the route. The position covers all the costs of hiring one archaeologist and one technician and all the expenses necessary to monitor them.

The calculation of executed works is carried out as lump sum according to the bid submitted by the Intermunicipal Institute for the Protection of Cultural Monuments of Subotica for all work and material and according to the abovementioned description.

- 1.2 EARTH WORKS

- HUMUS EXCAVATION

Excavation of humus should be done mechanically for about 95% and manually 5% within designed thicknesses and widths below and above the road-street road body. Once designed widths, grade of slopes and surveying terrain according to cross-section are marked, excavation of humus should start. The thickness of the removable humus layer is, as a rule, determined by the Design based on geomechanical testing and is determined on the spot together with the inspection body per profiles or road sections. If it is necessary to change thickness during construction, the supervisory authority will enter this change in the construction log. Humus must not interfere with the soil for the embankment, as well as to allow drainage of the road body, so it should be left far away from that pile. The excavated humus in the amount that will be used to resoil landscaping, road shoulders and slopes should be deposited in regular figures and the surplus prepared for transport.

Calculation of executed works is performed per cubic meter of removed autochthonous humus with pushing of up to 10 m, for all work and material.

- EXCAVATION IN A WIDE EXCAVATED HOLE BY A TRENCHER

This work covers wide excavations that can only be done with a trencher in relatively tight spaces, and which are foreseen by the Design or the request of the supervisory authority: in the cut, cut and fill, bore pit and larger deviations. The wide excavation should be done at designed spot levels and slopes according to cross-sections. Check the prominent cross-section markings before commencement of works on excavation. It is planned that 80% of the excavation will be done mechanically and 20% manually. The excavated soil material should be deposited or loaded.

Calculation of executed works is done per cubic meter of excavated material that is deposited or loaded into vehicles.

- SUBSOIL COMPACTION

After excavation of humus, subsoil is compacted under the embankment and excavation of the cut and fill. Use mechanical means for subsoil compaction. Subsoil compaction is required according to the standard Proctor procedure 100% of maximum laboratory compaction, and up to d=50 cm in depth. In the case that the required compaction cannot be achieved on certain places, the compaction will continue with the addition of sandy and gravel material until required compaction sizes are achieved. This additional work is not paid separately, but only costs related to the procurement of sandy and gravel material.

The calculation of executed works is done per square meter of compacted soil for all work, material and control testing.

- CONSTRUCTION OF EMBANKMENT MADE OF SAND

The position includes procurement, transport, spreading with rough sand planning and fine planning and compaction of formation level material with possible wetting.

According to the decision of the Detailed Construction Design, i.e. in accordance with the Design Solution of the Pavement Structure, the construction of the formation level includes:

- construction of a layer of minimum thickness d≥20 cm made of incoherent material. The thickness is determined in the Detailed Construction Design.

Execution

The formation level/capping layer is only constructed when the supervisory authority receives a lower layer.

Construction should not be carried out during frost, as well as in the case where there is a layer of ice or snow on the lower layer planum (subsoil embankment), or in case the lower layer is frozen.

Spreading, planning and compaction are done by machine.

Compaction should be carried out with appropriate means used for compaction of incoherent material.

The described works should be carried out up to the level given by the Detailed Construction Design.

Quality Control of Materials for Formation Level/Capping Layer Construction

Non-plastic sand, sandy gravel or other similar incoherent materials may be used to make the formation level.

Quality control of material for the formation level and assessment of suitability should be done according to the following regulations:

| SRPS U.B1.010 | - | sampling |
| --- | --- | --- |
| SRPS U.B1.012 | - | determination of soil moisture |
| SRPS U.B1.014 | - | determination of specific gravity |
| SRPS U.B1.016 | - | determination of mass per volume |
| SRPS U.B1.018 | - | defining granulometric composition |
| SRPS U.B1.020 | - | determination of flow and rolling limits |
| SRPS U.B1.038 | - | determination of the optimal water content |
| SRPS U.B1.042 | - | determination of Californian Bearing Ratio (CBR) |

Tests are carried out for each material change, i.e. every 2000 m2 of the formation level/capping layer.

Criterion for Evaluating the Suitability of the Applied Material for Construction of the Formation Level/Capping Layer

The material for construction of the formation level must meet the following criteria:

- maximum mass per volume by standard Proctor test

d>1600 kg/m3

- based on granulometric composition, the material should belong to the group of sand or sandy gravel

- in case of sand, the material must be non-plastic

- in the case of sandy gravel, the material may contain a maximum 12% of fractions of less than 0.074 mm, which are non-plastic or of low plasticity;

- the ratio of non-uniformity of granulometric composition

for sand U> 4

for sandy gravel U> 9

- maximum grain max  <60 mm

- laboratory Californian Bearing Ratio (CBR), compaction ratio

Sz = 100% in relation to the maximum dry mass per volume determined by the standard Proctor test (for sand), or at Sz=95% in relation to the maximum dry mass per volume determined by modified Proctor test (for sandy gravel), must be CBR> 10% .

Control of Treated and Compacted Formation Level/Capping Layer

Control of treated and compacted layer of the formation level is performed by determining the degree of compaction or compressibility modulus every 50 m' according to the following regulations:

| SRPS U.B1.010 | - | sampling |
| --- | --- | --- |
| SRPS U.B1.012 | - | determination of soil moisture |
| SRPS U.B1.016 | - | determination of soil bulk density |
| SRPS U.B1.046 | - | determination of compressibility modulus with circular plate |

Criterion for the quality of incorporation assessment

It is necessary to achieve a compaction ratio of Sz>100% in relation to the maximum dry bulk density determined by the standard Proctor test for sandy material, or Sz> 95% in relation to the maximum dry bulk density determined by modified Proctor test for sandy gravel material. The compressibility modulus should be Me≥25 MPa.

The Contractor bears the costs of tests that should be done again due to unsatisfactory results.

Criterion for evaluation of evenness

The formation level/capping layer must have a longitudinal grade and crossfall given by the Detailed Construction Design, i.e. the leveling spot levels surveyed on each cross-section must not deviate more than 30 mm.

The evenness of constructed formation level planum measured at each cross-section (left edge, axis, right edge) with a 4 m long measuring bar and a wedge must not have a depression greater than 30 mm.

Calculation of executed works is done per cubic meter of completed embankment in compacted condition for all work, material and control testing in accordance with the abovementioned description.

CONSTRUCTION OF EMBANKMENT MADE OF EARTH MATERIAL

Works on construction of embankment made of earth include backfilling of soil from the cut or taken from borrow pit, spreading, wetting or drying required, planning, compaction according to regulations and control testing. The embankment is made according to the designed cross-sections, spot levels and grades from the Design with deviations of up to 5 cm. The embankment should be made in layers that are up to 30 cm thick, with a grade for drainage. The embankment should be compacted by vibrating means or static rollers, with compaction until the required compaction is achieved. Quantities for embankment construction also include part of the embankment below the road shoulder. Compaction control of formed layers should be checked by a circular plate that is 30 cm in diameter, whereby a minimum value of the compressibility modulus Ms=25 MN/m2 is required.

Calculation of executed works is done per cubic meter of completed embankment in compacted condition for all work, material and control testing in accordance with the abovementioned description.

- PLANNING AND FORMATION LEVEL ROLLING

The process of making formation level consists of planning according to the designed levels and additonal compaction on the entire formation level width to the required compaction. Final rolling should be performed with a smooth roller to obtain a flat surface of the formation level, allowing deviations of (+, -) 2 cm relative to the designed levels. Compaction testing should be carried out with a circular plate d=30cm in diameter, requiring a minimum value of compressibility modulus Ms min = 25k MN/m2.

Calculation of performed works is done per square meter for all work and material, with control testing.

- RESOILING OF FLAT AND ASLANT SURFACES AND ROAD SHOULDERS

The work involves resoiling of flat surfaces, slopes of cut, embankment and road shoulder, with the necessary grassing, in 15-30 cm layers. Surface resoiling should be done using humus, which has been previously removed from the route and deposited in figures. If the humus in the landfill is dry, it should be spread and moistened with water when applied. After spreading and planning the layer of humus, it should be easily compacted. If there is not enough humus on the spot, the humus should be delivered from the borrow pit or from a place designated by the Supervisory authority. Delivery of materials from the borrowing pit is calculated separately according to the position of transportation of soil materials.

The calculation of the performed works is done per square meter of the humus and grass surface, and the cost of production includes all work and material.

- SPREADING EARTH MATERIAL AT THE LANDFILL

Surplus of humus and excavated earth material to the category brought to landfills, spread over the landfill in layers and roughly planned according to the supervisory authority.

The calculation of executed works is done per cubic meter of spread material, for all work and material.

- TRANSPORT OF EARTH MATERIAL

Surplus of excavated humus and earth material, and delivery of materials from the borrow pit for embankment or resoiling to the category, loading and transport to the landfill or to the place of installation, at a distance from the preliminary estimate of works. This position includes vehicle loading, transport, unloading and rough spreading.

Calculation of executed works is done per cubic meter of loaded, transported, unloaded and roughly distributed material.

- 1.3. PAVEMENT STRUCTURE

- CONSTRUCTION OF BASE COURSE MADE OF MECHANICALLY COMPACTED GRAIN STONE MATERIAL 0/63ММ

Description

The position includes procurement, transport, installation, rough and fine spreading, eventual wetting and compaction of the base course made of unbound stone material, according to the dimensions given in the Design.

Basic Materials

The basic material should be a mixture of crushed grains formed by crushing rocks, coarse natural grains, or artificial stone.

Quality of Material

The quality requirements are explained in detail in the standard SRPS EN 13242:2007-Aggregates for unbound or hydraulically bound materials for use in construction works and road construction.

Stone aggregate

The mixture of unbound stone aggregate is made up of fractions of crushed stone, gritting material, sand and fillers to provide required granulometric composition. Determination of particle size distribution is defined in standard SRPS EN 933-1: 2009.

Granulometric composition

The granulometric composition of the unbound stone aggregate should be within the following limits:

| Square hole of a sieve (mm) | Passage through sieves, per masses % crushed aggregate 0/63 mm |
| --- | --- |
| 0.063 | 0-3 |
| 0.125 | 2-15 |
| 0.25 | 5-20 |
| 0.5 | 7-26 |
| 0.71 | 9-30 |
| 1.0 | 11-34 |
| 2.0 | 18-44 |
| 4.0 | 26-56 |
| 8.0 | 36-69 |
| 16.0 | 50-85 |
| 22.4 | 59-93 |
| 31.5 | 72-100 |
| 45.0 | 85-100 |
| 56.0 | 90-100 |

and to satisfy the following requirements:

- coefficient of uniformity Cu > 6

- coefficient of curvature CC = 1 ÷ 3.

The presence of "fine" particles

The stone aggregate may have components smaller than 0.063mm (according to SRPS EN 13242: 2007) in the following quantity:

- up to 5% landfill (by weight)

- after placement up to 8% (by weight).

The content of stone grains up to 0.02 mm in size should not exceed 3% (by weight). The plasticity index of fine particles (smaller than 0.425mm) must be less than 6.

The sand equivalent shall be at least ES> 50 (in accordance with SRPS EN 933-8: 2008).

Mechanical properties of stone aggregate

The fracture resistance coefficient of crushing, determined by Los Angeles method (SRPS EN 1097-2: 2008), may not exceed 35%.

The resistance to freezing of stone grains, determined (pursuant to SRPS EN 1367-2: 2009) through testing with magnesium sulphate and expressed as the proportion of pealed particles in relation to the initial mixture of grains, may amount up to 25 m-%, and for testing with sodium sulphate – up to 5 m-%.

A maximum of 20 m.-% of grain is allowed in the aggregate where the shape does not meet the condition l:d  3:1 (tests according to EN 933-4). The content of organic mixtures in the aggregate should not colour the 3% sodium base solution darker than the reference colour (testing pursuant to SRPS EN 1744-1: 2009). Stone aggregate for the observed layer must not contain harmful low-quality grains or impurities (tests according to SRPS EN 1744-1: 2009).

The bearing capacity of aggregate, determined in the laboratory by the Californian Bearing Ratio (CBR) procedure, must be less than 80%.

Execution

Before commencement of works, it is necessary to check that machines and tools to be used meet the requirement to perform work in accordance with these technical conditions.

The installation of stone aggregates in the subject layer must be done mechanically. Manual installation is only permitted locally on places approved by the Supervisory Engineer. Any repair of the granulometric composition of aggregate at the site or place of installation must be approved by the Supervisory Engineer on the basis of relevant results of the preliminary testing.

The water quantity needed for ensuring the optimal aggregate humidity for better improved compression should be evenly added to the aggregate already in the location of procurement. If water must be added at the location of installation it is dosed by spraying, which prevents the rinsing off of the fine grains. During compression, the aggregate humidity may deviate from the optimal humidity by not more than ± 2 m.-%.

Spreading of stone aggregate for the subject layer must be carried out using adequate equipment. Spreading must be carried out on the same day as damping. Compression is carried out from the lower to the upper edge of the layer. The number of passages of the appropriate means of compression, which were previously defined in the pilot section, should be tested within the internal control of the density of the state of the compaction of the installed aggregate layer.

All irregularities discovered during compression should be repaired as detailed by the Supervisor. Prior to the completion of compression it is necessary to determine the bearing capacity of the installed sub-base.

If the values required in the project documents have not been achieved, the Contractor should ensure the quality of the installed sub-base by additional measures. The compacted layer must have designed spot levels, width and slope as given in the design.

Temporary Landfill

If the Contractor temporarily deposits fractions of stone aggregate prior to placement into the subject layer, then the landfill space must be previously and appropriately prepared (leveled, fixed, drained).

The temporary landfill should be as rectangular as possible (sides up to 50 m long). Stone aggregate should be spread in layers, homogenized and appropriately moistened in height of up to 3,0 cm. The grade of slope of the temporary landfill is 1: 2.

A temporary access road to the temporary landfill must be built.

The temporary landfill must be appropriately marked (location, number, size, phase when it is allowed to take it). Once temporary landfill has been taken, no new landfills must be brought there until it is fully utilized.

Quality of Execution

Compression

The state of compression of the sub-base aggregate, which is defined by the density tested with the Proctor’s procedure, should amount to at least 98 % on average.

Bearing capacity

Bearing capacity of made layer is determined by the static deformation modulus Ev2. Bearing capacity control is done by measuring the modulus of deformability by the circular plate method - SRPS U.B1.047: 1997. The required value of deformability modulus should be as follows:

| - Material type | - Thickness of base course made of crushed stone - (cm) | - Deformability modules Еv2 (MPa) |
| --- | --- | --- |
| - Crushed stone aggregate 0/63mm | - 30 | - ≥ 60 |

The required value of the deformability modulus ratio should be Еv2 / Еv1 < 2.2.

Flatness, Height, Slope

Unevenness of the sub-base high plain is determined by measuring the deviation below a laid 4-meter long lath, which is placed along any direction in relation to the road centre line. Allowed deviations are as follows:

Planum of the subject layer may deviate from the lath by no more than 20 mm (upper limit). If such deviations occur continuously one after another, the flatness should be repaired pursuant to the instructions defined by the Supervision.

The height of individual measuring points on planum of the layer should be determined by levelling. The planum of the layer at an arbitrary point should not deviate from the design elevation by more than ± 10 mm (upper limiting value).

The slope of the planum of the layer, in accordance with the Design Solution, should have equal crossfall and longitudinal slope of the pavement.

Quality Control of Execution

For each significant aggregate type planned for placement in the subject layer, it is necessary to determine the conformity with the requirements of the design documents and these technical conditions:

- at the beginning of placement, through preliminary tests

- during installation through testing within the internal and independent control.

Preliminary Tests

Preliminary tests for the inspection of conformity of the aggregate properties with the required ones specified in these technical conditions, namely:

- aggregate granulometric composition

- proportion of grains with a size of up to 0.063 mm

- form of particles/grains

- coefficients of uniformity and curvature

- sand equivalent

- resistance to crushing – Los Angeles coefficient

- percentage of organic admixtures

- bearing capacity – CBR procedure

Test pursuant to Proctor's modified procedure:

- optimal humidity

- maximum density

The results of preliminary tests should be adjusted to the details of the properties of the supplied aggregates provided by the Contractor.

Internal Control

The contractor’s internal control (which should be carried out by an authorized laboratory) should, during the installation of the sub-base aggregate, determine the aggregate’s conformity with the requirements of the project documents and these technical conditions. During the placement of aggregate in the sub-base, the laboratory should take and inspect the conformity of the properties with the minimum frequency.

Aggregate samples should be taken on the temporary storage site/landfill (twothirds of them) and from the installed subbase (one third of them). The minimum frequency of testing during the internal control of aggregate placement in the sub-base is defined:

| Properties | Minimum frequency of testing |
| --- | --- |
| Granulometric composition of aggregate mixture | 1000 m3 |
| Form of particles/grains |  |
| Coefficients of uniformity and curvature |  |
| Proportion of grains with a size of up to 0.063 mm |  |
| Plasticity of fine particles |  |
| Sand equivalent |  |
| Humidity and density by Proctor |  |
| Percentage of organic admixtures | 2000 m3 |

| Properties | Minimum frequency of testing |
| --- | --- |
| percentage of water and thickness | 200 m2 |
| bearing capacity: |  |
| - static deformation modulus Еv2 | 500 m2 |
| planum of the layer/layer high plain: |  |
| - evenness | 40 m1 |
| - height and slope | 40 m1 |

Independent Control- Control Testing

The scope of works of independent control during the sub-base constructions is, as a rule, in the ratio of 1:4 to those of internal control. The control testing should be carried out by an institution authorized by the Client. The location for aggregate sampling at the temporary storage site/landfill and during placement in the sub-base should be determined by the Supervisor through a statistical random selection.

Protection and Maintenance of the Constructed Layer

The Contractor should bear the costs and protect and maintain the constructed layer until the next layer is built. Maintenance involves adequate repair of any damage and should be carried out to such an extent and frequency that it ensures that the layer remains intact and in good condition. The repair should preserve the good flatness of the surface of the constructed layer.

Measuring and Payment

Calculation and payment are done per cubic meter (m3) of completed and received layer of designed thickness by the Supervisory Authority.

- CONSTRUCTION OF BASE COURSE MADE OF MECHANICALLY COMPACTED GRAIN STONE MATERIAL 0/31.5 ММ

Description

The position includes procurement, transport, installation, rough and fine spreading, eventual wetting and compaction of the base course made of unbound stone material, according to the dimensions given in the Design.

Basic Materials

The basic material should be a mixture of crushed grains formed by crushing rocks, coarse natural grains, or artificial stone.

Quality of Material

The quality requirements are explained in detail in the standard SRPS EN 13242:2007-Aggregates for unbound or hydraulically bound materials for use in construction works and road construction.

Stone aggregate

The mixture of unbound stone aggregate is made up of fractions of crushed stone, gritting material, sand and fillers to provide required granulometric composition. Determination of particle size distribution is defined in standard SRPS EN 933-1: 2009.

Granulometric composition

The granulometric composition of the unbound stone aggregate should be within the following limits:

| Square hole of a sieve (mm) | Passage through sieves, per masses % crushed aggregate 0/31.5 mm |
| --- | --- |
| 0.09 | 2-9 |
| 0.25 | 5-15 |
| 0.50 | 8-21 |
| 1.0 | 11-30 |
| 2.0 | 15-40 |
| 4.0 | 20-50 |
| 8.0 | 28-62 |
| 16.0 | 46-75 |
| 31.5 | 95-100 |
| 45.0 | 100 |

and to satisfy the following requirements:

- coefficient of uniformity Cu > 6

- coefficient of curvature CC = 1 ÷ 3.

The presence of "fine" particles

The stone aggregate may have components smaller than 0.063mm (according to SRPS EN 13242: 2007) in the following quantity:

- up to 5% landfill (by weight)

- after placement up to 8% (by weight).

The content of stone grains up to 0.02 mm in size should not exceed 3% (by weight). The plasticity index of fine particles (smaller than 0.425mm) must be less than 6.

The sand equivalent shall be at least ES> 50 (in accordance with SRPS EN 933-8: 2008).

Mechanical properties of aggregates

The fracture resistance coefficient of crushing, determined by Los Angeles method (SRPS EN 1097-2: 2008), may not exceed 35%.

The resistance to freezing of stne grains, determined (pursuant to SRPS EN 1367-2: 2009) through testing with magnesium sulphate and expressed as the proportion of pealed particles in relation to the initial mixture of grains, may amount up to 25 m-%, and for testing with sodium sulphate – up to 5 m-%.

A maximum of 20 m.-% of grain is allowed in the aggregate where the shape does not meet the condition l:d  3:1 (tests according to EN 933-4). The content of organic mixtures in the aggregate should not colour the 3% sodium base solution darker than the reference colour (testing pursuant to SRPS EN 1744-1: 2009). Stone aggregate for the observed layer must not contain harmful low-quality grains or impurities (tests according to SRPS EN 1744-1: 2009).

The bearing capacity of aggregate, determined in the laboratory by the Californian Bearing Ratio (CBR) procedure, must be less than 80%.

Execution

Before commencement of works, it is necessary to check that machines and tools to be used meet the requirement to perform work in accordance with these technical conditions.

The installation of aggregates in the subject layer must be done mechanically. Manual installation is only permitted locally on places approved by the Supervisory Engineer. Any repair of the granulometric composition of aggregate at the site or place of installation must be approved by the Supervisory Engineer on the basis of relevant results of the preliminary testing.

The water quantity needed for ensuring the optimal aggregate humidity for better improved compression should be evenly added to the aggregate already in the location of procurement.

If water must be added at the location of installation it is dosed by spraying, which prevents the rinsing off of the fine grains. During compression, the aggregate humidity may deviate from the optimal humidity by not more than ± 2 m.-%.

Spreading of stone aggregate for the subject layer must be carried out using pavers. Spreading must be carried out on the same day as damping. Compression is carried out from the lower to the upper edge of the layer. The number of passages of the appropriate means of compression, which were previously defined in the pilot section, should be tested within the internal control of the density of the state of the compaction of the installed aggregate layer.

All irregularities discovered during compression should be repaired as detailed by the Supervisor.

Prior to the completion of compression it is necessary to determine the bearing capacity of the installed sub-base. If the values required in the project documents have not been achieved, the Contractor should ensure the quality of the installed sub-base by additional measures.

The compacted layer must have designed spot levels, width and slope as given in the design.

Temporary Landfill

If the Contractor temporarily deposits fractions of aggregate prior to placement into the subject layer, then the landfill space must be previously and appropriately prepared to ensure good drainage system. A temporary access road to the temporary landfill must be built.

Quality of Execution

Compression

The state of compression of the sub-base aggregate, which is defined by the density tested with the Proctor’s procedure, should be greater than 98 %.

Bearing capacity

Bearing capacity of made layer is determined by the static deformation modulus Ev2. Bearing capacity control is done by measuring the modulus of deformability by the circular plate method - SRPS U.B1.047: 1997. The required value of deformability modulus should be as follows:

| - Material type | - Thickness of base course made of crushed stone - (cm) | - Deformability modules Еv2 (MPa) |
| --- | --- | --- |
| - Crushed stone aggregate 0/31mm | - 25 | - ≥ 90 |

The required value of the deformability modulus ratio should be Еv2 / Еv1 < 2.2.

Flatness, Height, Slope

Unevenness of the sub-base high plain is determined by measuring the deviation below a laid 4-meter long lath, which is placed along any direction in relation to the road centre line. Allowed deviations are as follows:

Planum of the sub-base may deviate from the lath by no more than 20 mm (upper limit). If such deviations occur continuously one after another, the flatness should be repaired pursuant to the instructions defined by the Supervision.

The height of individual measuring points on planum of the sub-base should be determined by levelling. The planum of the layer at an arbitrary point should not deviate from the design elevation by more than ± 10 mm (upper limiting value).

The slope of the planum of the layer, in accordance with the Design Solution, should have equal crossfall and longitudinal slope of the pavement.

Quality Control of Execution

For each significant aggregate type planned for placement in the subject layer, it is necessary to determine the conformity with the requirements of the design documents and these technical conditions:

- at the beginning of placement, through preliminary tests

- during installation through testing within the internal and independent control.

Preliminary Tests

Preliminary tests for the inspection of conformity of the aggregate properties with the required ones specified in these technical conditions, namely:

- aggregate granulometric composition

- proportion of grains with a size of up to 0.063 mm

- form of particles/grains

- coefficients of uniformity and curvature

- Plasticity of fine particles (finer than 0.425)

- sand equivalent

- resistance to crushing – Los Angeles coefficient

- percentage of organic admixtures

- bearing capacity – CBR procedure

Test pursuant to Proctor's modified procedure:

- optimal humidity

- maximum density

The results of preliminary tests should be adjusted to the details of the properties of the supplied aggregates provided by the Contractor.

Internal Control

The contractor’s internal control (which should be carried out by an authorized laboratory) should, during the installation of the sub-base aggregate, determine the aggregate’s conformity with the requirements of the project documents and these technical conditions. During the placement of aggregate in the sub-base, the laboratory should take and inspect the conformity of the properties with the minimum frequency.

Aggregate samples should be taken on the temporary storage site/landfill (twothirds of them) and from the installed subbase (one third of them).

The minimum frequency of testing during the internal control of aggregate placement in the sub-base is defined:

| Properties | Minimum frequency of testing |
| --- | --- |
| Granulometric composition of aggregate mixture | 1000 m3 |
| Form of particles/grains |  |
| Coefficients of uniformity and curvature |  |
| Proportion of grains with a size of up to 0.063 mm |  |
| Plasticity of fine particles |  |
| Sand equivalent |  |
| Humidity and density by Proctor |  |
| Percentage of organic admixtures | 2000 m3 |

| Properties | Minimum frequency of testing |
| --- | --- |
| percentage of water and thickness | 200 m2 |
| bearing capacity: |  |
| - static deformation modulus Еv2 | 500 m2 |
| planum of the layer/layer high plain: |  |
| - evenness | 40 m1 |
| - height and slope | 40 m1 |

Independent Control- Control Testing

The scope of works of independent control during the sub-base constructions is, as a rule, in the ratio of 1:4 to those of internal control.

The location for aggregate sampling at the temporary storage site/landfill and during placement in the sub-base should be determined by the Supervisor through a statistical random selection.

Protection and Maintenance of the Constructed Layer

The Contractor should bear the costs and protect and maintain the constructed layer until the next layer is built. Maintenance involves adequate repair of any damage and should be carried out to such an extent and frequency that it ensures that the layer remains intact and in good condition. The repair should preserve the good flatness of the surface of the constructed layer.

Measuring and Payment

Calculation and payment are done per cubic meter (m3) of completed and received layer of designed thickness by the Supervisory Authority.

- CONSTRUCTION OF BITUMINOUS REGULATING COURSE

Bituminous base course is a bearing course in pavement structure made of a mixture of stone material, rock dust and bitumen as a binder. According to the largest grain size, it is divided into DBNS 22, DBNS 32 and DBNS 45.

According to the type of stone material used and depending on the design structure and intended bearing capacity, it is divided into:

DBNS A, made on the basis of crushed separated stone material according to JUS B.B3.100 (aggregate), with the addition of rock dust as required;

DBNS B, made on the basis of crushed separated stone material with at least three fractions and a maximum grain size of 45 mm, with the addition of rock dust as needed;

DBNS C, made of crushed stone material that is not separated with the correction of stone material, or not separated natural unbound material with the addition of at least 30% of crushed stone mixture above 4 mm and up to 45 mm, with correction by the addition of sand or rock dust;

DBNS D, made of completed natural unbound material with a maximum grain size of 45 mm, with composition correction by the addition of sand or rock dust.

Rock material, sand and rock dust must meet requirements of JUS. There should be no organic matter in the mineral mixture. The granulometric composition of the mixture must be such that it meets prescribed sieving curves of the standard.

Bitumen BIT 60 and BIT 90 are used as the binder. The exact proportion of bitumen is determined by making the previous composition of the mixture and is approximately 3.3-5.2% depending on the type.

Prior to commencement of work, all material to be used must be tested in a laboratory, which must comply with the technical requirements for the production of JUS.U.E9.020 bases. The preparation of the mass/compound is done by modern asphalt bases and the installation with pavers with required rolling combined with rubber and smooth rollers. Transport of masses should be done by tippers equipped for unloading. During the preparation and installation of the mass, it is necessary to carry out all control testing, material testing and asphalt masses in accordance with the standards. The layers must be constructed in the design thicknesses and the designed crossfalls and longitudinal slopes. Control tests of produced asphalt mass shall be performed for each 1500 t of mass produced, namely: bitumen percentage, granulometric composition, stability, stability and deformation ratio, content of voids and void occupancy with bitumen. Control testing of the built-in layer is performed every 2,000 m2 of the constructed layer, namely: percentage of voids, the degree of compression and the thickness of the layer.

The calculation of the executed works is done per square meters of the upper surface of the actually done layer. The price includes all costs of material procurement, production and installation of asphalt, transport, equipment, preliminary and control testing and all other costs required for the execution of works.

Exceptionally, when it comes to leveling the existing pavement surface during the reconstruction of traffic surfaces, the calculation can also be made per tonne or m3 of installed mass.

- CONSTRUCTION OF BITUMINOUS BASE COURSE (BNS 22А)

Description

The position includes procurement, preparation, placement and compaction of a mixture of granulated mineral material and bitumen, in two layers according to the design.

Basic Materials

The following basic materials should be used to form the upper base course of bituminous material:

- crushed carbonate stone material 0/4; 4/8; 8/16 and 16/22 mm;

- rock dust of carbonate composition;

- bitumen BIT 35/50

Quality of Basic Materials

Fine Crushed Aggregate

Fine crushed aggregate must be composed of a carbonate rock mass having the following characteristics:

Physical properties

- Resistance of coarse grains (10/14) to freezing- magnesium sulfate (m.-%)............ MS18

- wearing according to Los Angeles (%)....................................................................... LA30

- Resistance of coarse grains during polishing............................................................. PSV30

- Water absorption in coarse grains  4/8 mm (%).............................................................1,2

- Coating of coarse grains with bitumen binder (%)..............................................  min 80

- Geometrical properties

- quality of fine particles (d > 0.125mm) (g/kg)...................................... MBF10/up to 5

- shape of coarse grains (d > 2mm) (m.-%)...................................................................... FI20

- Proportion of crushed grains in the mixture of coarse grain (m.-%)................................. C90/1

- proportion of fine particles (≤ 0.063) size fractions 4/8 (m.-%)..........................................f2

coarse  ............................................................f2

- fine/mixed...........................................................f10

- The curve of granulometric composition must be such that the curve lies in the following limiting region:

| - Size of the sides of the sieve opening - mm | - Passage through the sieve in - % of mass BNS 22А |
| --- | --- |
| - 0,063 - 0,25 - 0,71 - 2,00 - 4,00 - 8.00 - 11,20 - 16,00 - 22,40 - 31,5 | - 4-14 - 7-37 - 12-53 - 21-65 - 30-74 - 44-85 - 54-92 - 70-100 - 97-100 - 100 |

- Rock dust

Rock dust must meet the criteria given in SRPS B.B3.045 for the first class quality.

Bitumen

Bitumen must be BIT 35/50. Bitumen must comply with the criteria given in SRPS EN 12591: 2013.

Mixture

Bitumen content should be approximately 3.5% in the asphalt mixture. The exact content of bitumen will be determined in the previous composition of the asphalt mixture. The sieving lines of mineral mixture should lie within the limits given in the previous points. The characteristics of trial bodies according to Marshall’s method shall be as follows:

- content of voids (v.-%) ........................................................................................  4-7

- void occupancy in the mineral mixture with bitumen (%)...................... 55-77

- sensitivity to water

minimum value of indirect tensile strength (%)..........................................ITSR80

- Proportional rut depth (10 000 cycles at 60ºС)

in accordance with SRPS EN12697-22……………………………………….....max 7%

- Rolling (compression) of a layer (%)......................................................................   98

Embedded Layer Properties

Layer Thickness

The average layer thickness of bituminous mixture in the base course may be up to 15% less than the designed or contracted layer thickness (ultimate limit value).

The average total thickness of the layer of bituminous mixtures in the wearing and base course may be up to 5% less than the designed or contracted total layer thickness (ultimate limit value). If the average total layer thickness, determined from the thicknesses of the individual layers is less than the contracted thickness, due to the insufficient thickness of the built-in wearing, binder and/or base course, the Client may ask for deductions.

Thickness of bituminous mixture in the wearing or base course may be up to 10% greater than the maximum designed thickness.

- Evenness of the layer

The evenness of the high plain of the asphalt base course should be determined – in an arbitrary direction in relation to the road centre line – as a deviation below a laid 3 m long measuring rod, or by another adequate measurement method (SRMG, i.e. EN 13036-7).

The limiting deviation values of the high plain of the bituminous mixtures installed in the base course are:

- in one layer.......................... ≤ 8 mm

- in two layers (on the bottom layer).......   ≤ 10mm

- Execution Technology

- Substrate Preparation

The asphalt layer can be laid on a substrate that is dry and in no way frozen. Before commencement of works on paving, the substrate must be well cleaned with steel brushes and blown out by the compressor. After cleaning the substrate, the supervisory authority will survey the finish grade and evenness of the substrate. The flatness measurement procedure is defined in EN 13036-7. For parts where the surface of the substrate layer deviates from prescribed height for more than +15 mm, it is necessary for the contractor to repair the substrate according to the requirements of the design solution, namely:

-  on places where the surface of the substrate is below prescribed finish grade, repair should be carried out by increasing the layer of asphalt mixture with asphalt concrete- wearing course;

- on places where the surface of the substrate is above prescribed finish grade, surplus of asphalt mass in the substrate should be removed by countersink.

To ensure the adherence of the layers the substrate should be sprayed with a bituminous emulsion (unstable cation emulsion at 60-70% of bitumen content). The quantity of the spraying emulsion depends on the substrate condition and it should be adjusted to each individual condition. The informative quantity of the spraying emulsion amounts to 0.3 to 0.5 kg/m2.

- Preparation and Transport of Asphalt Mixture

- The asphalt machine must have a sieve with the opening of 22.4 mm that will remove impermissible coarse grains in the mineral mixture. The bitumen temperature should be from 150 to 160 °C. The aggregate temperature must not be higher than the bitumen temperature for more than 15 °C. The temperature of asphalt mixture in the mixer should be within 150 - 170 °C (extremely 175 °C). The temperature measurement of hot bituminous mixture must be carried out in accordance with EN 12697-13.

- Placement of Asphalt Mixture

- Temperature of the asphalt mixture at the site of placement should not be lower than 145 °C and higher than 175 °C.

Weather Conditions during Installation

The bituminous base course according to the specifications of these technical conditions can be installed during the period when the air temperatures are higher than 5 °C, without wind or min 10 °C with wind. The installation of asphalt mixture must not be done when it is haze or rain. The substrate temperature must not be lower than + 5 °C.

- Quality Control

- Preliminary Tests of Asphalt Mixture

- Prior to commencement of work, the Contractor is obliged to prepare in the authorized laboratory a design of the preliminary asphalt mixture in accordance with the requirements of these technical conditions. Work must not start until the Contractor proposes a preliminary mixture for approval by the supervisory authority. Certificates of basic materials and preliminary mixture should not be older than 6 months. In case of changes in the basic materials or changes in the choice of materials, the Contractor is obliged to submit to the supervisory authority a proposal for changing the adopted asphalt mixture in a written form, or to propose a new preliminary mixture for approval, before using these materials.

- Proven Construction Composition of Asphalt Mixture

- The quality of preliminary asphalt mixture is proved by trial work with the fact that the asphalt mixture is adopted at the site itself and the quality of installation on the test road section. If the quality of basic materials on the site does not meet these technical conditions, the Contractor is obliged to provide new quality basic materials. If dosage of the base materials, according to the preliminary mixture, cannot meet all prescribed requirements for physical and mechanical properties of asphalt mixture and for the built-in layer, it is necessary to correct the dosage of the base materials and repeat the test. Only when all set requirements have been fulfilled by the trial work, will the supervisory authority adopt the construction mixture and give its approval for continuous operation. Proven construction composition of asphalt mixture is performed by an authorized laboratory.

Quality Control

The control of the quality and conformity of bituminous mixtures comprises constant internal and independent controls of the production and installation activities, pursuant to the provisions in EN 13108-21 and the requirements stipulated by these technical conditions.

All direct impacts on the quality and requirements for an assessment of the conformity of the produced and installed bituminous mixtures should be stated in the quality rules.

The locations for sampling of the produced bituminous mixtures at the construction site and the installed bituminous mixtures for the asphalt base and wearing courses, as well as the point of measurement of the required properties of the bituminous mixtures, should be defined by a statistic random selection. The following internal control tests of the basic inbound material properties, i.e. properties of the aggregate grains and bituminous binder, should be carried out.

- - aggregate mixture for every 300 t:

- - rock dust: of the same manufacturer

- aggregate mixture for every 500 t:

- - sand: of the same manufacturer

- proportion of fine grains for 500 t:

- - crushed aggregate: every fraction at – aggregate composition

- - proportion of fine grains

- - form of grains (ratio 1: 3)

- bituminous binder: of the same manufacturer every tanker or at least once a day for each type:

- - penetration at 25 C

- softening point pursuant to PK procedure

Internal control of produced bituminous mixture includes:

- Inspection of the temperature at 500 t of the produced bituminous mixture; inspection of the composition and the mechanical and spatial properties of the produced bituminous mixture

- of the same type at 500 t:

- - proportion of binder

- - extracted aggregate composition

- - content of overall voids in the bituminous mixture

- - content of voids in the aggregate

- - void occupancy in the aggregate with binder

The properties of the bituminous mixtures installed in the asphalt wearing course should be checked with the following internal control tests of the installed asphalt surfacing on cores for every 500 t:

- layer thickness

- layer adherence (if required)

- layer density

- content of voids in the layer

on the layer for every 500 m2

- density measured by a non-destructive method

- smoothness of high plain measured by a 3-meter rod

- high plain height determined by levelling and high plain slope.

Conformance Assessment

- Upon completion of individual works or stages of works within the execution of asphalt courses, it is necessary to carry out statistical analyses of the results of the internal and independent control of:

- - inbound materials,

- - the produced bituminous mixture and

- - the installed bituminous mixture.

- The contractors of both the internal and independent control should prepare a statistical analysis of the control testing results, each of them for their own activities. The statistical analyses and their comparison represent a basis for the assessment of the quality conformance and for potential claims and measures.

- The assessment of conformance of the results of all the control tests with the requirements in the contractual documentation and technical conditions should be prepared by the inspection authority responsible for the independent control and submitted to the supervising engineer.

- Criteria for Calculation of Executed Works

- The quantities of executed works determined should be calculated according to the contracted unit prices. The unit price should take into account all services needed for the complete execution of the asphalt base and wearing course. The contractor may not demand additional payments, unless agreed otherwise in the contract. If the contractor fails to ensure the quality within the required values, and if the deductions from his payment have already been calculated, all of his contractual liabilities referring to the warranty should remain in force.

Deductions Due to Inadequate Quality

Deductions should be determined either on the basis of the inadequate average value for the works executed or on the basis of inadequate individual defined values. The higher deduction value should be relevant.

In the case that:

- the proportion of the bituminous binders in the bituminous mixture is too small, or

- there are too many voids in the installed asphalt course, the higher deduction value should be relevant.

Executed Works

Due to:

- a small percentage of bituminous binder in the bituminous mixture, which is defined in the requirements for bituminous mixture composition,

- inadequate content of voids in the installed layer of bituminous mixture,

- small thickness of the executed asphalt course,

- poor adhesion of the installed asphalt courses, and

- inadequate evenness of the high plain of the executed asphalt course,

the client may calculate deductions. The ultimate limiting values, i.e. deviations from the limiting value, are given in the following table.

| Characteristic properties | Unit of measure | Deviation from the limiting value |
| --- | --- | --- |
| - percentage of bituminous binder | m.-% | - 0,3 |
| - content of voids in the installed bituminous mixture | V.-% | 2 |
| - thickness of the installed asphalt course | % | -15 |
| - adhesion of the installed asphalt courses | % | - 25 |
| - evenness of high plain of the installed asphalt course |  |  |
| - 3 m rod or | mm | +6 |
| - IRI | mm | 0,6 |

Deduction Evaluation

Deductions of the executed works should be evaluated according to the Special Technical Conditions for the pavement structure issued by PE Roads of Serbia from 2012.

Measurement and Payment

Calculation is done per m2 of completed asphalt layer of a certain thickness according to this description.

- CONSTRUCTION OF A WEARING COURSE – ASPHALT CONCRETE (АB11S)

Description

The position includes procurement, preparation, placement and compaction of asphalt concrete. The base for preparation of technical conditions for this position is SRPS U.E4.014.

Basic Materials

- noble fine crushed aggregate 2/4 mm, 4/8 mm, 8/11 mm;

- crushed sand 0/2 mm (carbonates)

- rock dust of carbonate composition

- bitumen  BIT 50/70

Quality of Basic Materials

Fine Crushed Aggregate

Fine crushed aggregate must be composed of a carbonate rock mass having the following characteristics:

Physical properties

- Resistance of coarse grains (10/14) to freezing- magnesium sulfate (m.-%)............ MS18

- wearing according to Los Angeles (%)....................................................................... LA20

- Resistance of coarse grains during polishing............................................................. PSV50

- Water absorption in coarse grains  4/8 mm (%).............................................................1,2

- Coating of coarse grains with bitumen binder (%)..............................................  min 90

- Geometrical properties

- quality of fine particles (d > 0.125mm) (g/kg)...................................... MBF10/up to 5

- shape of coarse grains (d > 2mm) (m.-%)...................................................................... FI20

- Proportion of crushed grains in the mixture of coarse grain (m.-%)................................. C100/0

- proportion of fine particles (≤ 0.063) size fractions 2/4 (m.-%)................................................f4

fractions 4/8 (m.-%).....................................................f2

coarse..........................................................................f1

- fine/mixed..................................................................f10

- Chemical properties

- Proportion of coarse organic admixtures (m.-%).......................................................... mLPC0.5

- Sand

For sand, fine crushed sand obtained from a rock mass of carbonate or silicate composition may be used.

The granulometric composition of the sand must satisfy the following conditions:

| Sieve opening in | Passage through sieve in % weight |
| --- | --- |
| mm | Crushed sand 0/2 mm |
| 0,09 0,25 0,71 2 4 | 0-10 * 15-35 40-85 90-100 100 |

*/    If the proportion of fine particles in the sand grain mixture is higher than 10% by mass, the fine particles should comply with the requirements for fillers defined in SRPS U.E4.014: 90.

Sand must also satisfy the following characteristics:

- sand equivalent................................................................................... at least SE60

- There should be no clumps of clay in the sand

- Sand should not contain organic impurities

- No clumps of sticky particles may form in the sand

- Rock Dust

Carbonate stone quality according to SRPS B.B3.045 shall be applied for rock dust. Rock dust made of ground dolomitic rock is not desirable because of its poor adhesion to bitumen. Prior to commencement of works, the Contractor must obtain a certificate of quality of rock dust from the authorized laboratory that will guarantee quality according to the standard SRPS B.B3.045 (I quality).

Bitumen

BIT 50/70 should be applied for the binder with: softening point (ring and ball PK 46-54oC), penetration 50-70, and penetration index greater than -1.5 to +0.7, paraffin content max 2% and ductility min 100 cm. Other properties are according to SRPS EN 12594.

Mineral Mixture Composition

The proportion of basic fractions in the mineral mixture should be adjusted so that the sieving line is as follows:

| Sieve and sift openings | Preliminary testing and machine trial operation |
| --- | --- |
|  | Passages through sieve and sift in % of weight |
| 0,063 0,25 0,71 2 4 8 11,2 16,0 | 6-9 10-18 16-30 31-48 45-65 70-88 90-100 100 |

Composition of Asphalt Mixture

The orientational composition of asphalt mixture is as follows:

- filer 0-0,09 mm ...............................................  - 8 %

- sand 0,09-2 mm ................................................  -30 %

- fine crushed aggregate 2-11 mm ...................................  - 62 %

All:          100%

- binder BIT 50/70 - the amount of binder required for the asphalt mixture to meet required conditions is determined in the previous composition of the asphalt mixture.

The optimum amount of bitumen in the asphalt mixture should not be less than 5.0%, to prevent rapid fatigue of asphalt concrete. For fine crushed aggregate originating from rock masses that use a small amount of bitumen for wrapping, so that the optimum bitumen amount is below 5.0%, the upper limiting value in the zone of filler and sand should be applied, and the lower limiting value in the fine crushed aggregate area.

Physical-mechanical properties of asphalt mixture

The asphalt mixture prepared according to EN 13108-1 must meet the following conditions:

| Ord.no. | Testing procedure | Quality conditions |  |  |
| --- | --- | --- | --- | --- |
|  |  | Preliminary and construction mixture | Control testing |  |
| 1. | Residual voids %(v/v) | 3 – 6.5 | 3 – 6.5 |  |
| 2. | Voids in mineral mixture filled with binder, %(v/v) | 65 -80 | 65 -80 |  |
| 3. | Resistance to permanent deformation (%) | PRDAIR5.0 | PRDAIR5.0 |  |
| 5. | Sensitivity to water, minimum value of indirect tensile strength (%) | ITSR80 | ITSR80 |  |
| 7. | Tolerance of aggregate composition in samples for control testing in relation to the values in the initial composition | sieve 0,09 mm sieve 0,25 mm sieve 0,71 mm sieve 2,0 mm sieve 4,0 mm sieve 8,0 mm | Individual samples | Average of four samples |
|  |  |  | ± 1.5 ± 2 ± 3 ± 4 ± 4 ± 4 | ± 1 ± 1.5 ± 2 ± 3 ± 3 ± 4 |
| 8. | Tolerance of deviation of binder quantity in relation to adopted recipe | Determined by the preliminary tests and tolerance is within ± 0,3 m, -% of the value determined in the previous composition of the asphalt mixture |  |  |

Properties of Built-in Wearing Course

- Compression

- Rolling (compression) of the layer (%)......................................................................   98

- Content of voids

- Content of voids in the layer (v/v,%)......................................................................  2.0 - 8.5

Layer Thickness

The average layer thickness of bituminous mixture in the wearing course may be up to 25% less than the designed or contracted layer thickness (ultimate limit value). The average total thickness of the layer of bituminous mixtures in the wearing and base course may be up to 5% less than the designed or contracted total layer thickness (ultimate limit value). If the average total layer thickness, determined from the thicknesses of the individual layers is less than the contracted thickness, due to the insufficient thickness of the built-in wearing, binder and/or base course, the Client may ask for deductions. Thickness of bituminous mixture in the wearing or base course may be up to 10% greater than the maximum designed thickness.

- Planum/High Plain of the Asphalt Wearing Course

- Evenness

The evenness of the high plain of the asphalt wearing course should be determined – in an arbitrary direction in relation to the road centre line – as a deviation below a laid 3 m long measuring rod, or by another adequate measurement method (SRMG, i.e. EN 13036-7). The limiting deviation values of the high plain of the asphalt bituminous layers are:

- in one layer.......................... ≤ 4 mm

- Slope

- The high plain slope of the asphalt wearing course should be equal to the crossfall and longitudinal slope of the pavement. Permitted deviations of should not exceed ± 0.2 % total.

- Execution Technology

- Substrate Preparation

The asphalt layer can be laid on a substrate that is dry and in no way frozen. Before commencement of works on paving, the substrate must be well cleaned with steel brushes and blown out by the compressor. After cleaning the substrate, the supervisory authority will survey the finish grade and evenness of the substrate. The flatness measurement procedure is defined in EN B 13036-7.  For parts where the surface of the substrate layer deviates from prescribed height for more than +15 mm, it is necessary for the contractor to repair the substrate according to the requirements of the design solution, namely:

-  on places where the surface of the substrate is below prescribed finish grade, repair should be carried out by increasing the layer of asphalt mixture with asphalt concrete- wearing course;

- on places where the surface of the substrate is above prescribed finish grade, surplus of asphalt mass in the substrate should be removed by countersink.

To ensure the adherence of the layers the substrate should be sprayed with a bituminous emulsion (unstable cation emulsion at 60-70% of bitumen content). The quantity of the spraying emulsion depends on the substrate condition and it should be adjusted to each individual condition. The informative quantity of the spraying emulsion amounts to 0.3 to 0.5 kg/m2.

- Preparation and Transport of Asphalt Mixture

- The production of asphalt mixture is done mechanically. Temperature of bitumen in the tank should be in range from 150 to165oC. The delivery dynamics of bitumen should be coordinated with the production of asphalt mixture, so the binder should be placed in storage as soon as possible. The aggregate temperature must not be higher than the bitumen temperature for more than 15 °C. The temperature of asphalt mixture in the mixer should be within 150 - 170 °C (not more than 175 °C). The temperature measurement of hot bituminous mixture must be carried out in accordance with EN 12697-13. The asphalt mixture is ​​transported in a truck that is covered with awning to prevent cooling and soiling of the mixture. A sufficient number of trucks must be provided by the Contractor, so that asphalt mixture is transported without any problems and finisher operates without interruption. The truck basket for transport of the asphalt mixture must be clean and sprayed with substance for the prevention of the bituminous mixture sticking to things (silicone emulsion or solution of potassium soap in water) before each filling. The use of petroleum products for spraying truck baskets is not permitted.

- Placement and Compression of Asphalt Mixture

The asphalt mixture AB11s is ​​installed with a pavers. Temperature of the asphalt mixture during installation neither must be less than 1400 nor higher than 1750C. The asphalt mixture should not be installed if it does not have required temperature.

Compaction of the asphalt mixture should be done in a classic way combining static and pneumatic rollers. Vibration is not allowed. Static rollers 6-8t, static rollers 12-16t and rubber-wheeled rollers 12-16t are used for compaction. A total of 4 to 5 rollers are required. The rollers must have a device that ensures spraying of the drum surface with a silicone emulsion. The use of oil derivatives for spraying of wheels is not allowed. The method of rolling shall be determined when designing the pilot section and shall be such as to achieve prescribed layer compaction. Self-adhesive bituminous strip must be used on all transverse or longitudinal joitns of the wearing course where paving is interrupted. Self-adhesive tapes/strips are bituminous mechanically made thermoelastic profiles that adhere to the existing asphalt layer. They are used for longitudinal or transverse composition/joint of the wearing course, when works are not carried out in the full width of the pavement or where paving is interrupted.

The process of execution of works involves:

- Edge preparation

- Installation of bituminous strip/tape

- adhesion of bituminous strip/tape

Edge Preparation - With self-adhesive bituminous tape/strip, it is necessary to thoroughly clean and dry surface where it is necessary to apply primer (approximately 15g/m). Primer drying time at 20º C is 2-3 minutes.

Installation of self-adhesive bituminous tape/strip - Place the strip along the edge with the adhesive side up

Adhesion of bituminous strip/tape - Fit the tape with the white adhesive side and glue it tightly to the edge. Particular attention should be paid to the fact that the strip must be placed at least 5 mm above the surface of the existing asphalt, so that when rolling, two layers are joined evenly after the new one is applied.

Weather Conditions during Installation

The bituminous base course can be installed during the period when the air temperatures are higher than +5 °C, without wind or min +10 °C with wind. The installation of asphalt mixture must not be done when it is haze or rain. The substrate temperature must not be lower than + 5 °C.

- Quality Control

- Preliminary Tests of Asphalt Mixture

- Prior to commencement of work, the Contractor is obliged to prepare in the authorized laboratory a design of the preliminary asphalt mixture in accordance with the requirements of these technical conditions. Work must not start until the Contractor proposes a preliminary mixture for approval by the supervisory authority. Certificates of basic materials and preliminary mixture should not be older than 6 months. In case of changes in the basic materials or changes in the choice of materials, the Contractor is obliged to submit to the supervisory authority a proposal for changing the adopted asphalt mixture in a written form, or to propose a new preliminary mixture for approval, before using these materials. The report on the preparation of previous composition of the asphalt mixture shall include:

- information on the origin, quality and characteristics of constituent materials,

- data on the percentage of fraction of stone material in mineral or asphalt mixture,

- granulometric composition of the mineral mixture,

- diagram of granulometric composition of the mineral mixture,

- physical-mechanical properties of asphalt mixture samples with five percent binder,

- optimum binder content and

- diagram of changes in the physical-mechanical properties of asphalt mixtures depending on the binder content.

- Certificates of compliance of component materials not older than 6 months must be attached to the Report on Preliminary Composition. For aggregates, there must be a valid certificate from an authorized laboratory and according to the "Order on the mandatory certification of fractionated aggregate for asphalt and concrete" published in the Official Gazette of SFRY no. 41 of June 19th,1987.

- Proven Construction Composition of Asphalt Mixture

The construction composition of asphalt mixture must be determined before commencement of works. The construction composition of the asphalt mixture serves as proof that it is possible to produce the asphalt mixture of quality on the asphalt plant, which was designed by the preliminary composition of the asphalt mixture. A prerequisite for proving the previous composition of an asphalt mixture is ​​to check the quality of constituent materials stored on the asphalt base.

The production of an asphalt mixture shall be deemed to have been demonstrated when at least three samples of the asphalt mixture taken from continuous production show that:

• granulometric composition of the rock mixture is within the tolerance prescribed in these technical conditions;

• the binder content for each sample is within the tolerance of 0.3% (m/m) of the value given in the previous composition of the asphalt mixture; and

• physical-mechanical properties of all samples satisfy the conditions prescribed in these technical conditions.

The construction composition of asphalt mixture is given in the form of a written report.

If the construction composition of asphalt mixture on the asphalt plant cannot be fully incorporated into allowed deviations, the preliminary composition of the asphalt mixture must be corrected with the consent of the Designer.

The preliminary composition of the asphalt mixture needs to be re-designed if it cannot be proven on the asphalt plant due to significant differences in the composition and properties of the asphalt base constituent materials or due to the specificity of the asphalt plant.

Quality Assurance

Quality assurance includes preliminary quality control, checking of work force and internal and control tests, all as described in these technical conditions.

Ongoing Testing

Ongoing testing is performed by the Contractor. In the case that the Contractor does not have the appropriate equipment and staff, the on-site inspection is carried out, at the contractor's expense, at a laboratory registered for that type of control.

- Laboratory equipment for ongoing testing

The laboratory must have all equipment for required tests, for ongoing testing in the production process as well as for testing during the preparation of the construction asphalt mixture defined by these technical conditions. As part of the ongoing testing, the constituent materials and the asphalt mixture are tested as follows:

- bitumen BIT 50/70 (PK, penetration),

- rock dust (granulometric composition),

- crushed sand (granulometric composition),

- fine crushed aggregate 2/4, 4/8 and 8/11 (granulometric composition),

- granulometric composition of the rock mixture, binder content in the asphalt mixture and

- Physical-mechanical characteristics of the asphalt mixture.

Samples of the asphalt mixture shall be taken at the place of production or at the place of installation from the hot newly spread asphalt mixture behind the paver. Control of compaction, voids and thickness is done by extracting asphalt samples (cores) at the same place where the sample of hot asphalt mixture is taken.

The scope and frequency of ongoing tests must be such as to ensure equal quality in accordance with these technical conditions, namely:

- ongoing tests of rock dust, crushed sand and fine crushed aggregate is carried out for every 300 t of asphalt produced,

- ongoing bitumen testing is carried out at the beginning and every 25 t of bitumen consumed and

- ongoing testing of the composition and physical-mechanical characteristics of the asphalt mixture is ​​determined for every 300 t of asphalt mass produced.

Quality Control

The control of the quality and conformity of bituminous mixtures comprises constant internal and independent controls of the production and installation activities, pursuant to the provisions in EN 13108-21 and the requirements stipulated by these technical conditions.

All direct impacts on the quality and requirements for an assessment of the conformity of the produced and installed bituminous mixtures should be stated in the quality rules. The locations for sampling of the produced bituminous mixtures at the construction site and the installed bituminous mixtures for the asphalt base and wearing courses, as well as the point of measurement of the required properties of the bituminous mixtures, should be defined by a statistic random selection. The following internal control tests of the basic inbound material properties, i.e. properties of the aggregate grains and bituminous binder, should be carried out.

- - aggregate mixture for every 300 t:

- - rock dust: of the same manufacturer

- aggregate mixture for every 500 t:

- - sand: of the same manufacturer

- proportion of fine grains for 500 t:

- - crushed aggregate: every fraction at – aggregate composition

- - proportion of fine grains

- - form of grains (ratio 1: 3)

- bituminous binder: of the same manufacturer every tanker or at least once a day for each type:

- - penetration at 25 C

- softening point pursuant to PK procedure

Internal control of produced bituminous mixture includes:

- Inspection of the temperature at 500 t of the produced bituminous mixture; inspection of the composition and the mechanical and spatial properties of the produced bituminous mixture

- of the same type at 500 t:

- - proportion of binder

- - extracted aggregate composition

- - content of overall voids in the bituminous mixture

- - content of voids in the aggregate

- - void occupancy in the aggregate with binder

Internal control of produced bituminous mixture includes:

- Inspection of the temperature at 500 t of the produced bituminous mixture; inspection of the composition and the mechanical and spatial properties of the produced bituminous mixture

- of the same type at 500 t:

- - proportion of binder

- - extracted aggregate composition

- - content of overall voids in the bituminous mixture

- - content of voids in the aggregate

- - void occupancy in the aggregate with binder

The properties of the bituminous mixtures installed in the asphalt wearing course should be checked with the following internal control tests of the installed asphalt surfacing on cores for every 500 t:

- layer thickness

- layer adherence (if required)

- layer density

- content of voids in the layer

on the layer for every 500 m2

- density measured by a non-destructive method

- smoothness of high plain measured by a 3-meter rod

- high plain height determined by levelling and high plain slope.

Conformance Assessment

- Upon completion of individual works or stages of works within the execution of asphalt courses, it is necessary to carry out statistical analyses of the results of the internal and independent control of:

- - inbound materials,

- - the produced bituminous mixture and

- - the installed bituminous mixture.

- The contractors of both the internal and independent control should prepare a statistical analysis of the control testing results, each of them for their own activities. The statistical analyses and their comparison represent a basis for the assessment of the quality conformance and for potential claims and measures.

- The assessment of conformance of the results of all the control tests with the requirements in the contractual documentation and technical conditions should be prepared by the inspection authority responsible for the independent control and submitted to the supervising engineer.

- Criteria for Calculation of Executed Works

- The quantities of executed works determined should be calculated according to the contracted unit prices. The unit price should take into account all services needed for the complete execution of the asphalt base and wearing course. The contractor may not demand additional payments, unless agreed otherwise in the contract. If the contractor fails to ensure the quality within the required values, and if the deductions from his payment have already been calculated, all of his contractual liabilities referring to the warranty should remain in force.

Deductions Due to Inadequate Quality

Deductions should be determined either on the basis of the inadequate average value for the works executed or on the basis of inadequate individual defined values. The higher deduction value should be relevant.

In the case that:

- the proportion of the bituminous binders in the bituminous mixture is too small, or

- there are too many voids in the installed asphalt course, the higher deduction value should be relevant.

Executed Works

Due to:

- a small percentage of bituminous binder in the bituminous mixture, which is defined in the requirements for bituminous mixture composition,

- inadequate content of voids in the installed layer of bituminous mixture,

- small thickness of the executed asphalt course,

- poor adhesion of the installed asphalt courses, and

- inadequate evenness of the high plain of the executed asphalt course,

| Characteristic properties | Unit of measure | Deviation from the limiting value |
| --- | --- | --- |
| - percentage of bituminous binder | m.-% | - 0,3 |
| - content of voids in the installed bituminous mixture | V.-% | 2 |
| - thickness of the installed asphalt course | % | -25 |
| - adhesion of the installed asphalt courses | % | - 25 |
| - evenness of high plain of the installed asphalt course |  |  |
| - 3 m rod or | mm | +4 |
| - IRI | mm | 0,6 |

the client may calculate deductions. The ultimate limiting values, i.e. deviations from the limiting value, are given in the following table.

Deduction Evaluation

Deductions of the executed works should be evaluated according to the Special Technical Conditions for the pavement structure issued by PE Roads of Serbia from 2012.

Measurement and Payment

Calculation is done per m2 of completed asphalt layer of a certain thickness according to this description.

- CONSTRUCTION OF A WEARING COURSE – ASPHALT CONCRETE (АB11)

Wearing course made of asphalt concrete is made from a mixture of crushed stone material, rock dust and bitumen as a binder. According to the nominal grain size, it is divided into: AB 4, AB 8, AB 11, AB 16 and AB 22.

According to the granulometric composition of the stone mixture asphalt concrete is divided into:

Wearing course of a wider granulometric composition of rock mixture AB4 - AB16

Wearing course of a narrow range of granulometric composition of rock mixture: AB11s - AB22s

Rock material, sand and rock dust must meet requirements of JUS. Stone material must have eruptive origin for roads with heavy truck traffic.There should be no organic matter in the mineral mixture. The granulometric composition of the mixture must be such that it meets prescribed sieving curves of the standard.

Bitumens BIT 60 and BIT 90 are used as binders, while AB4 and AB11 and bitumen BIT130 are used for fine grained asphalt concrete. The exact proportion of bitumen is determined by making the previous composition of the mixture and is approximately 4.5 - 8.0%  depending on the type.

Prior to commencement of work, all material to be used must be tested in a laboratory, which must comply with the technical requirements for the production of of asphalt concrete. The preparation of the mass/compound is done by modern asphalt bases and the installation with pavers with required rolling combined with rubber and smooth rollers. Transport of masses should be done by tippers equipped for unloading. During the preparation and installation of the mass, it is necessary to carry out all control testing, material testing and asphalt masses in accordance with the standards.

The layers must be constructed in the design thicknesses and the designed crossfalls on a clean substrate. Control tests of produced asphalt mass shall be performed for each 500 t of mass produced (5000 m2) for roads with heavy truck traffic and 600 t (6,000 m2) for other roads, namely: bitumen percentage, granulometric composition, stability, stability and deformation ratio, content of voids and void occupancy with bitumen. Control testing of the built-in layer is performed every 2,000 m2 of the constructed layer, namely: percentage of voids, the degree of compression and the thickness of the layer.

The calculation of the executed works is done per square meters of the upper surface of the actually done layer. The price includes all costs of material procurement, production and installation of asphalt, transport, equipment, preliminary and control testing and all other costs required for the execution of works.

Exceptionally, when it comes to leveling the existing pavement surface during the reconstruction of traffic surfaces, the calculation can also be made per tonne or m3 of installed mass.

- CONSTRUCTION OF CONCRETE ROAD SURFACING

Above properly constructed and prepared substrates, make a concrete road surfacing in the layer of designed thickness. Use permanent natural gravel, sand or crushed material taken from the river for aggregate and they must comply with technical conditions for aggregate according to JUS B.B3.050. Only concrete RS 350 according to JUS B.C1 should be used for concrete construction and water used for making concrete must be clean and tested beforehand. Concrete must be made mechanically and in that way dosing of each component must be ensured. The concrete mixture is transported to the place of placement by vehicles which prevent the segregation process. Lay foil over finely planned, well-compacted and prepared substrate, so that the individual strips cover at least 5 cm in the direction of crossfall. Installation of concrete mass must be done by machine, high-frequency vibrating paver. Regarding two-layer surface dressing, layers are usually made of concrete of different qualities. The top layer should not be thick less than 5 cm. After concreting, transverse and longitudinal joints should be performed mechanically. The width of transverse joints should be 14-18 mm and the length 20 mm. The concrete pavement must be protected from drying due to wind and sun and from wetting due to rain. No traffic shall be allowed for seven days after the pavement has been constructed, and the joints must be filled with grouting compound JUS N.M3.095 only after the pavement has completely become solid. During the construction of concrete road surfacing, all preliminary tests, tests during construction and finished pavement are subject to the technical conditions of JUS U.E3.020.

Calculation of the executed works is done per square meter of completed concrete pavement for all work and material with necessary tests and other costs.

- CONSTRUCTION OF ROAD SURFACING USING CONCRETE PREFABRICATED ELEMENTS

Plan a 3 cm thick sandy layer over the constructed and tested blanket course. Finished concrete elements are laid on the sandy layer. Lay concrete elements manually compressing the sandy layer. Evenness of removed surfaces should be controlled by a 4m lath/rod. Each parking space, for the purpose of marking, is separated by concrete beams, which are paid according to the special position of these technical conditions. The laid concrete elements should be rolled with a light static roller in two directions. Once concrete elements have been laid, fill the void with humus that has compost. Fill voids manually without compaction of humus into the holes. After filling with humus, clean the surface with sharp brooms. The quality of the construction material used should be in accordance with the applicable JUS standards.

The calculation of the executed works is done per meter required for all work and material.

- LAYING CONCRETE CURBS

Work involves laying concrete curbs with the most common dimensions 18/24, 12/18 and 6/20. Curbs are laid on the prepared concrete base of MB 20, according to the Design. Some details about the excavation, concrete substrates, laying concrete, joints pointing and the rest should be done according to the details of the Design. Grouting of joints that are 1 cm wide should be carried out with cement mortar, which is made in a ratio of 1:3. The height and position of the curb must be in accordance with the design. Curbs must be MB 40 and have certificates of quality required. Only curbs without damages can be installed.

Calculation of the executed works is performed per running meter along the curb, for all work and materials, including procurement and transport of curbs.

- DETERMINATION OF „ZERO STATE PAVEMENT STRUCTURE“ OF COMPLETELY CONSTRUCTED /REHABILITATED PAVEMENT STRUCTURE ON THE MAIN ROUTE OF THE ROAD

All measurements planned by determination of "zero state pavement " are done on wearing course on completely constructed pavement.

"Zero state pavement condition" included the following examinations:

      - Bearing capacity of the road structure testing using "Falling Weight deflectometer"-(FWD), with at list 7 geophones in the deflection basin d (1/1000mm). Measurement should be carried out in every lane, at every 100m. Testing should be carried out in accordance with the document: Technical Specifications -QCP RRSP- Edition 01, Belgrade 2017, Item 7.1.1. (Page 120/145).

      - Measurement of longitudinal roughness (IRI, m/km). Required quality of the device, the criteria for evaluating unevenness and frequency of testing should be in accordance with the document: Technical Specifications - QCP RRSP- Edition 01, Belgrade 2017, Item 7.1.2. (Page 120/145).

- Measurement of skid resistance testing (the Pendulum test-SRT) and measurement of pavement surface macrotexture by laser beam, should be in accordance with the document: Technical Specifications - QCP RRSP- Edition 01, Belgrade 2017, Item 7.1.3. (Page 120/145). Deviations from the proposal given by the abovementioned document are the need to carry out measurements, measure skid resistance using SRT pendulum and measurement of pavement surface macrotexture. In the case of applying an alternative method of measuring the macrotexture of the pavement (blasting method) then the Designer's opinion is required regarding the scope and method of measurement as well as the required criteria.

      - Surveying condition of pavement surface with high resolution digital camera. Required quality of the device, the criteria for assessing the state of deterioration of the road surface and the frequency of testing should be in accordance with the document: Technical Specifications - QCP RRSP- Edition 01, Belgrade 2017, Item 7.1.4. (Page 120/145).

      - Pavement structure surveying with GPR - Ground Penetrating Radar. The frequency of testing should be in accordance with the document: Technical Specifications - QCP RRSP- Edition 01, Belgrade 2017, Item 7.1.5. (Page 120/145).

Calculation of the executed works is done as lump sum according to the position of performed tests for all work and material and equipment.

- 1.4 DRAINAGE SYSTEM

- CONSTRUCTION OF DRAINAGE DITCHES WITHOUT LINING

The drainage ditch, without lining, is done by excavating the soil according to the details of the Design or according to the provisions of the supervisory authority, in all soil categories. All excavation surfaces of the bottom and sides of the ditch shall be flat in the prescribed slopes of the bottom and slopes. Excavation should be done mechanically and manual labor should be minimized and applied only where it cannot be done mechanically. Ditch excavation is measured in cubic meters of really excavated soil.

The calculation of the executed works is done per cubic meter of ditch and the unit price includes excavation, planning of the ditch surface and depositing of the excavated material.

SLOPE STAKING OF EXISTING CANALS

Slope staking of existing canals is done by excavation of soil according to the project details or according to the provisions of the supervisory authority in all soil categories. All excavation surfaces, the bottom and sides of the ditch shall be flat in the prescribed falls and slopes. Excavation should be done mechanically and manual labor should be minimized and applied only where it cannot be done mechanically. Existing ditches that collapse during construction must be re-arranged in accordance with the position and dimensions shown in cross-sections.

The calculation of the executed works is carried out per running meter of the existing or cleaned canal, and the unit price includes excavation, embankment, planning of the canal surface as well as all transport (with loading and unloading).

2.  TECHNICAL CONDITIONS FOR EXECUTION OF WORKS ON TRAFFIC SIGNAGE

The technical conditions for the execution of works are in accordance with the Rulebook on Traffic Signalization and specification of works in Technical Design. The position numbers in the technical conditions for execution are aligned with the position numbers in the Rulebook on Traffic Signalization.

The Contractor must provide the supervisory authority with the appropriate documents: certificate on the quality of foil classes 1 and 2 and 3, the certificate on the quality of the road sign panel and their compliance with the standard SRPS EN 12899 (Official Gazette of the RS No.85 /2017 Article 16 minimum conditions):

1. safety factor values class (PAF1)

2. wind load values class ( WL5)

3. dynamic pressure of snow class (DSL1)

4. the greatest temporary deformation (TDB4), issued by an accredited laboratory.

Traffic signage must be made in accordance with Technical instructions no. BS-02/2013 and BS-03/2013.

Elements of traffic signage are:

1.	ROAD SIGNS
2.	ROAD MARKINGS

6.	ILLUMINATED MARKINGS ON THE ROAD
7.	ROAD EQUIPMENT

8.	TECHNICAL DEVICES FOR SLOWING DOWN TRAFFIC

10.	OTHER WORKS

- The technical conditions for the production, procurement and installation of individual elements of traffic signalization are explained through the individual positions of these works.

- The ordering of traffic signage elements is done on the basis of specification of the works in the Design.

- The design of individual elements is carried out on the basis of European regulations, SRPS standards, the Rulebook on Traffic Signage ("Official Gazette of the RS" No. 85/2017, hereinafter referred to as the Rulebook), as well as detailed drawings in the Design. In the process of designing road signs, manufacturers of them are obliged to comply with the provisions of the Technical Instruction (with binding application) on the method of testing and the procedure for assessing the conformity of road signs on state roads of the Republic of Serbia with the requirements of standards defined and adopted by PE "Roads of Serbia", Belgrade.

- Road sign background requirements: for all road signs including structural strengthening, the road sign background shall be gray in accordance with RAL 7043, with a minimum coating thickness of 12 μm (in accordance with EN 13523-1).

- Road sign structure requirements: Road signs with an area that does not exceed 1.1 m2 must be made from one part. Road signs with a surface area exceeding 1.1 m2 can be constructed from parts, with necessary structural strengthening at the back of the sign.

- Installation, i.e. execution of individual elements of traffic signage is done on the basis of situational solution, cross-sections and other drawings from the Design, as well as on the basis of the Rulebook on Traffic Signalization and SRPS standards.

1.	ROAD SIGNS

Road signs shall be made of materials and in the manner prescribed by the Regulations. Standard road signs are made of the following materials:

- galvanized steel sheet with curved edge (abbreviated PCLPI),

- aluminum sheet (abbreviated AL),

- aluminum sheet strengthened with the clamps (abbreviated ALO),

- aluminum sheet with a curved edge (abbreviated ALPI).

- The use of aluminum materials with a tensile strength of at least 155 N/mm2 for road signs with curved edges and in an extruded aluminum profile (clamp), or a minimum of 200 N/mm2 for straight signs, is permitted for the production of road signs.

- Materials that comply with DIN EN 573-1 and 573-2, or materials with the following markings may be used:

- EN AW 52 51 H 24/H 34,

- EN AW 30 05 H 22/ H 49,

- EN AW 57 54 H 22/H 34/H 42.

- Aluminum materials may be used to make parts of sign assemblies and extruded elements that comply with DIN EN 573-3, or materials with the following markings:

- EN AW 60 60 T 4/T 66,

- EN AW 60 05 A/T 6.

Face of the road sign, with all symbols, letters and numbers according to the numbers of Article 14 Rulebook on Traffic Signalization, must have reflective properties:

- on the highway: signs set along the pavement shall be made of material of at least class 2 if there is no public lighting and materials of class 3 shall be used for traffic management signs if public lighting exists and signs posted on portals shall be of material class 3;

- on the motorway: signs set along the pavement shall be made of material of at least class 2, signs posted on portals shall be of material class 3;

- on other state and municipal roads: signs are made of material class 2;

- streets: signs are made of materials class 1.

In exceptional cases only in paragraph 1, Aricle 14:

- on the highway and motorway, class 2 materials are used in the production of signs beside objects on the road: III-58, III-59, III-60, III-61, III-90, III-90.1;

- on other roads, apart from streets, class 3 materials are used in the production of signs: I-32, I-33, I-34, I-34.1, I-35, II-1, II-2, III-5, III-6, III-7;

- on streets, class 2 materials are used in the production of signs: I-32, I-33, I-34, I-34.1, I-35, II-1, II-2, III-5, III-6, III-7;

- class 3 materials are used in the production of signs: III-11, III-28, III-85, III-86, III-89, III-89.1, III-89.2;

- class 1 materials are used in the production of signs: II-40, II-41, II-41.1, II-42, III-19 III-20, III-21, III-22, III-98 and III-99.

Since the subject of processing are sections in settlements and traffic nodes of the reference system located on the state road, the Design envisages the installation of standard road signs for this category of road in accordance with the Rulebook on Traffic Signalization, Technical Recommendation and SRPS standard. Based on the abovementioned, road signs have the following sizes:

1.1	Danger warning signs:

- Triangular with sides of 90 cm;

- Rectangular: 120x60 cm;

- Rectangular: 30x100 cm;

1.2	Regulatory signs:

- Triangular with sides of 90 cm;

- Circle Ø 60 cm in diameter;

- Circle Ø 40 cm in diameter;

1.3	Informative signs:

- Square with sides 60 cm;

- Square with sides 50 cm;

- Rectangular: 60x90 cm;

- Rectangular: 80x60 cm;

- Rectangular: 35x30 cm;

- Circle Ø 60 cm in diameter;

1.4	Additional panels:

- Square with sides 60 cm;

- Rectangular: 60x30 cm.

- Road signs along the road outside the settlement are placed at a height of 1,20 to 1,40 m.

- Road signs next to the road are placed on intersections in the settlement, outside pedestrian areas, depending on the number of signs, at a height of 1,4m to 1,8m, and on pedestrian areas in height of 2,2m to 2,4m.

- Installed signs must be secured against turning and shearing.

- Placed signs must be regularly maintained.

- Signs are placed, so that their plane deviates from the horizontal one by 3 to 5º in the field from the normal on the road axis.

- The position of the sign in the cross-section is determined by the Design.

- Road signs are placed on the column next to the pavement on the right, in the direction of movement.

- The height is calculated from the road surface to the lower edge of the road sign.

- Exceptionally, signs II-45 (mandatory passing by on the right side), II-45.1 (mandatory passing by on the left side) and II-45.3 (passing by on both sides) are placed in height of 1.4m.

- By exception of the above paragraph, signs placed at a height of 80 cm are signs: I-35 (approaching a railroad crossing without barriers or semibarriers), III-98 (road kilometres) and III-99 (road number, road section number and road kilometres).

- Exceptionally, signs: III-84 and III-84.1 (board for marking the tip of the delineator island) are placed in height of 0,5 m.

- The distance between the edge of the carriageway and the most prominent edge of the traffic sign placed on a road, intersection and in a settlement, outside of pedestrian areas, is 0,75 to 1,50 m. Exceptionally, it is 0,5m if there is a safety barrier and if traffic profile has stopping lanes.

- The distance between the edge of the carriageway and the most prominent edge of the traffic sign placed on pedestrian areas is from 0,30 m to 1,5 m.

- The manufacturer must guarantee the consistent quality of the sign for at least 5 years from the date of installation, i.e. 7 years from the date of production.

- The manufacturer is obliged to write the code of the sign from the Design on the back of the sign, and the code must be on the cover if the sign is wrapped.

QUALITY CONTROL

The manufacturer must hold a certificate of compliance for all materials used in the production of standard road signs. Quality control is performed in accordance with SRPS Z.S2.300.

CALCULATION OF WORKS

The price of the road sign includes procurement, delivery and transport to the contracted place of delivery at the request of the Contractor, all elements for fastening to the carrier (strengthening, clamps, boot bolts/screws, etc.), as well as quality control.

The calculation for each type of work is done per a piece (piece) of road sign.

1.7   Installation of road signs on posts/poles carrying road signs

By placing two signs on the same post, for different directions, the back parts of II-1 and II-2 must not be covered.

Mounting the sign on the built-in carrier (the price includes transport of the sign and workers from the checkpoint to the place of work, placing and fixing the sign to the pole by tightening the clips and cutting the nuts so that they cannot easily move. Procurement of a sign with transport from the manufacturer to the checkpoint is not included in the price).

1.8   Poles carrying road signs

The position covers production, procurement and installation of road sign carriers:

1.8.1	Single Tubular Posts

- Tubular posts are made of steel pipe of uniform cross-section and thickness, depending on the number and type of sign to be placed on the carrier, which is indicated in the specifications, namely bill of quantities of carriers in the Design.

- All metal parts of the carrier and structure should be protected by hot zinc with a thickness of 60 µm. The support posts must be protected from corrosion by artificial resin paint or plastic that is not painted, but it is a dark gray.

- The pole must be protected from rain on the upper side, i.e. sealed with a plastic plug or welded.

- The single tubular post must be secured against turning with the stave/rail at the base.

- The posts are laid in concrete foundations of MB 20 quality.

- Excavate the foundation pit and then pave the foundation of the pole, filled with concrete MB 20, together with the steel pole.

QUALITY CONTROL

The manufacturer must hold a certificate of compliance for all materials used in the production of poles carrying road signs.

CALCULATION OF WORKS

The price of single and truss posts includes the following works:

- procurement of road sign carriers, as well as quality control

1.9   Construction of foundation and installation of poles carrying road signs

1.9.1   Construction of road sign foundation

The foundation is composed in two stages:

- Earthworks - include excavation of soil or other material, for foundations, transport to landfill or spreading of material to the surrounding terrain. Works are calculated per m3 of excavated material.

- Concrete works - procurement, transport and installation of concrete, min MB 20 for tubular posts.

1.9.2   Installation of poles carrying road signs

- installation of road signs in concrete footing and mounting of the pole on the foundation. (includes transport of poles and workers from the point to the place of work, placement of the poles in casted foundation, fixing the post until concrete hardens).

The calculation for each type of work is done per piece (pcs) of the pole carrying road sign and concrete footing for the road signs.

2.	ROAD MARKINGS

Road markings are marked on roads with modern road surfacing. The application of materials for their implementation is set out in Table 1.

Road markings applied:

  - Longitudinal markings SRPS U.S4.222, SRPS U.S4.223 and SRPS U.S4.224

  - Transversal markings SRPS U.S4.225, SRPS U.S4.227 and SRPS U.S4.228

  - Other markings SRPS U.S4.229 to SRPS U.S4.233

- The process and equipment for applying road markings must be such that work does not affect the safe traffic flow and the safety of the Contractor.

- The equipment must allow the application of reflective beads by sprinkling (spraying), which significantly contributes to the durability of the markings visibility at night. If paint with pre-mixed glass beads is used, beads must also be applied on the surface.

- The width, colors and rhythm of interruption are given on the situation in the graphical part of the Design.

- Material, execution technology and other color properties are prescribed by SRPS Z.S2.240.

- Road markings are made as thick-layer road markings - thickness of a dry layer of the marking (coating) should be more than 0.80 mm.

- Road markings are executed with white and yellow paints, but the road markings must not increase the skiddiness of the carriageway.

- Road markings are made in greasy, permanent color for this type of work and paint carefully without breaking or smearing.

- The composition of material and the method how the markings are executed must be such as to provide reflective properties of the markings, as defined in Table 1.

- Road markings must retain at least 85% of their surface area at the end of the warranty period and at the end of that period shall not have lower retroreflection values than those given in Table 1 (in accordance with the Rulebook).

- The edges of lines and figures must be sharp and straight, with deviations from the designed line no more than 5 mm. The tolerance for deviations from the given measures given in the Design is a maximum of 5%.

- After applying road markings, time when traffic can flow over the marking, i.e. the duration of traffic restriction over the pavement, may not exceed 45 minutes.

- Yellow colour is used to mark the bus stop. The color for execution of the abovementioned elements should be made on the basis of natural and artificial resins with addmixtures. The color must have reflective properties achieved by the addition of reflective beads of at least 100 grams per 1 kilogram of color.

- Cold plastic (agglomerate) is used in the area of schools for the execution of "X" sign, the inscription "SCHOOL" and rumble strips, as well as for the marking of the pavement at node 1307 (the intersection of state roads IB 13 and IB 15) as indicated in the Site Plan.

- The work is done mechanically and manually.

Table 1. Material characteristics for execution of permanent road markings

| Type of road |  | RL White | RL Yellow | RW (if markings of Type 2 are applied) | Qd white | S*** (SRT units) |
| --- | --- | --- | --- | --- | --- | --- |
| Highway | *New markings | ≥300 | - | ≥100 | ≥160 | ≥50 |
|  | Minimum permitted value during exploitation | ≥150 | - | ≥50 | ≥130 | ≥45 |
| I class state road, not a highway | *New markings | ≥300 | ≥200 | ≥75 | ≥160 | ≥50 |
|  | Minimum permitted value during exploitation | ≥150 | ≥100 | ≥35 | ≥130 | ≥45 |
| II class State road | *New markings | ≥200 | ≥150 | ≥50 | ≥130 | ≥50 |
|  | Minimum permitted value during exploitation | ≥100 | ≥80 | ≥35 | ≥100 | ≥45 |
| municipal roads | *New markings | ≥200 | ≥150 | ≥50 | ≥130 | ≥50 |
|  | Minimum permitted value during exploitation | ≥100 | ≥80 | ≥35 | ≥100 | ≥45 |
| Main roads in a residential area | *New markings | ≥200 | ≥150 | ≥75 | ≥130 | ≥50 |
|  | Minimum permitted value during exploitation | ≥100 | ≥80 | ≥35 | ≥100 | ≥45 |
| Secondary roads in a residential area | *New markings | ≥150 | ≥100 | - | ≥130 | ≥50 |
|  | Minimum permitted value during exploitation vrednost godine | - | - | - | ≥100 | ≥45 |
| RL – retroreflection coefficient (mcd x m-2 x lux-1); RW – retroreflection coefficient in wet conditions (mcd x m-2 x lux-1); Qd – illumination coefficient under diffused lighting (mcd x m-2 x lux-1); S – resistance to sliding value (SRT) |  |  |  |  |  |  |

- Works are carried out in dry weather conditions at air temperature +10 ºC to +30 ºC, relative humidity of 85% maximum and pavement temperature +5 ºC to +45 ºC

- Before applying the paint, the pavement surface must be completely dry, clean, without dust and residual salt. Oil and other grease stains must be removed.

QUALITY CONTROL

The quality control of materials used from the paint of executed works is carried out according to SRPS U.S2.240. For all paint works, the warranty period must be at least 12 months.

The quality of the executed markings must be verified and certified in one of the recognized laboratories.

Other materials must meet the requirements for a certain durability and quality, and for each material the Contractor must provide a certificate.

The quality control of used colors and the work executed is carried out according to SRPS U.S2.240. The guarantee period for all works must be at least 12 months.

CALCULATION OF WORKS

The cost of works on road marking is calculated per square meter (m2) of marked area. The specification also shows total lengths of longitudinal pavement markings. The price includes field measurement, pavement cleaning and degreasing, marking and quality control of materials used and works executed according to SRPS EN 1436 standard and SRPS U.S2.240.

6.	ILLUMINATED MARKINGS ON THE ROAD

This position covers the production, procurement and installation of the following traffic equipment:

6.1 Illuminated markings on the road for marking the edge of pavement

6.1   Illuminated markings on the road for marking the edge of pavement

Direction signs

DESCRIPTION OF POSITION

The position covers the development, procurement and installation of direction signs. The number of direction signs is shown in the bill of quantities and the preliminary estimate of works.

MATERIALS

With their shape, dimensions, and manner of manufacturing, directional signs and markings must be visible in all weather conditions, and especially in cases of low visibility (night, fog, snow, etc.). Direction signs are set up to allow road users to detect road contours at night and in conditions of poor visibility.

EXECUTION AND ASSEMBLING

Direction signs are placed according to the Site Plan in the Design. Direction signs are set according to applicable standards with reflective fields of material Class 2. Directional signs must have reflecting bodies of a certain surface (foils or other reflecting bodies), as follows: red on the right, white on the left, in the movement direction of the vehicles. Direction signs are made according to the standard SRPS.Z.S2.235.

QUALITY CONTROL

The Contractor shall, before installation of direction signs, prove their quality with a certificate of compliance, which shall be presented to the supervisory authority.

CALCULATION OF WORKS

The signpost price includes the following works:

procurement of direction signs per a piece (pcs);

placement of direction signs per piece (pcs). (The direction sign price includes: transport of direction signs and workers from the checkpoint to the place of work, manual installation, direction signs placement).

Catadioptres

Only night markings reflecting body-catadioptre are placed on special posts made of metal or plastic - prisms, which are installed in the groove of the safety barrier, so as to make the prescribed angle on stretches where there is a safety barrier for vehicles.

Catadioptres whose colour is the same as the colour of direction signs (red-white) are placed in the groove of the safety barrier.

If the safety barrier is in the alignment, the catadioptres are:

- on protective safety barriers of levels H1 and N2 at a distance of 12 m;

QUALITY CONTROL

The Contractor shall, before installation of catadioptres, prove their quality with a certificate of compliance, which shall be presented to the supervisory authority.

CALCULATION OF WORKS

The catadioptre price includes the following works:

procurement of catadioptre is per a piece (pcs);

placement of catadioptre is per piece (pcs). (The catadioptre price includes: transport of catadioptre and workers from the checkpoint to the place of work, manual installation, catadioptre placement).

7.	ROAD EQUIPMENT

7.2   Safety barrier

DESCRIPTION OF POSITION

The position includes preparation, procurement and installation of steel safety barrier for vehicles, in accordance with Serbian standards. The type of barrier is determined within the bill of quantities of this Design, according to the classification given in the Technical Instructions for the Implementation of the Vehicle Restraining System on the State Roads of the Republic of Serbia issued by PE Roads of Serbia and the standard SRPS EN 1317.

MATERIALS

The material for the construction of each element of the safety barrier must comply with the requirements of the standard SRPS EN 1317.

EXECUTION AND ASSEMBLING

The safety barrier is placed according to the situations in the Design. Length of safety barrier/fence, microlocation where it is placed, the length of the end treatment, etc. is explicitly determined on the Site Plan.

The protective barrier of the fence is assembled on posts of appropriate length, so that the upper edge of the barrier is in height of 0.75 m from the nearest edge of the carriageway lane.

The fence must be protected against corrosion by galvanizing and the investor should choose that. End treatments of the fence in shape and length must meet technical requirements for installation given in SRPS EN 1317. The length of the end treatments is defined on the Site plan.

Reflecting bodies-catadioptres, whose color is the same as the colour of direction sign posts, are built into the safety barrier groove at a distance of 12 meters.

The distance between the posts is 2.0 and 1.33 m.

End treatments of the fence are carried out by lowering and partially burying them in the ground, and their length is defined in the Site Plan.

QUALITY CONTROL

The Contractor shall, prior to the installation of the safety barrier/fence, prove its quality with a certificate of compliance, which shall be presented to the supervisory authority.

CALCULATION OF WORKS

The price of the fence is calculated per running meter of the fence installed. The price of end treatments and transition structures is calculated per piece.

7.5 Pedestrian Railings

DESCRIPTION OF POSITION

The position covers the execution, procurement and installation of: pedestrian railings with foundations.

MATERIALS

The metal pedestrian railing is made of steel in accordance with the requirements of the standard.

The foundations are made of concrete with the minimum mark MB 20.

EXECUTION AND ASSEMBLING

The metal pedestrian railing should be installed, as well as standard traffic posts and must be protected against corrosion by hot-dip galvanizing in accordance with standard EN ISO 1461.

The metal pedestrian railing should be positioned according to the Site plan.

QUALITY CONTROL

The manufacturer must hold a certificate of compliance for all materials used in production of the specified traffic equipment.

CALCULATION OF WORKS

The price of the metal pedestrian railing includes the price of delivery and transport to the place of installation, ground preparation, placement and leveling, as well as quality control of the materials used.

8.	TECHNICAL DEVICES FOR SLOWING DOWN TRAFFIC

8.1   Acoustic speed bars

Acoustic speed bars are technical devices for slowing down traffic, which produce stronger vibrations and sound effects that warn drivers to reduce speed, or to harmonize driving with the prescribed speed limit, when vehicles cross them.

The position includes the production, procurement and installation of technical devices for slowing down traffic, hereinafter referred to as acoustic speed bars, at a distance of (3x2 lanes), 3m long, d=12cm wide. Acoustic speed bars are set in pairs at a distance of 1.8 m (2.0 m) and if necessary can be repeated several times.

Acoustic speed bars are made of cold plastic. Cold plastic must be resistant to all weather conditions, UV rays, petroleum products, oils, salts and abrasion (wear).

Acoustic speed bars must have necessary certificates of compliance from competent institutions and/or laboratories to prove their technical characteristics and to guarantee the possibility of their use in the function of designing technical devices for slowing down traffic.

The price is calculated per running meter of placed bar. The price is stated per running meter, as well as the installation price, which includes all necessary work, as well as all costs required for installation according to the model ‘’turnkey construction contract’’, which implies that once works are completed by the Contractor, traffic can flow normally and safely at places where acoustic speed bars are installed.

10. OTHER WORKS

10.1. Dismantling and removal of road signs and advertising panels

DESCRIPTION

The Contractor is obliged to safely remove all the elements of the sign, connection accessories and sign, remove the post with concrete foundation and fill the hole of the foundation and bring the road shoulder into proper condition. All elements of the damaged post and old foundation must be removed to a location designated by the supervisory authority. All dismantled elements are transported to the Client’s warehouse at the request of the Supervisory Authority, while the surplus material created by demolition or removal is transported to the landfill designated by the Supervisory Authority.

MEASUREMENT AND CALCULATION

The cost of works includes all works required to complete them with all the costs of loading and unloading, dismantling and transport, as well as repairing the road shoulder, while the calculation is done per piece.

10.3. Dismantling and removal of safety barriers

DESCRIPTION

The Contractor is obliged to safely remove all existing elements of the safety fenece/barrier, connection accessories and posts. The dismantled fence and its damaged elements with the elements of the foundation posts must be removed to a place designated by the supervisory authority.

MEASUREMENT AND CALCULATION

The cost of works on dismantling of the safety barrier/fence is made per running meter with all costs of loading and unloading, dismantling and transport, as well as repairing the road shoulder.